Quantachrome NovaWin - Data Acquisition and Reduction

 for NOVA instruments

 ?1994-2010, Quantachrome Instruments

 version 11.0

Analysis Report

Operator:open Date:2014/10/07 Operator:open Date:10/7/2014

Sample ID: L3 Filename: C:\QCdata\Physisorb\sttn\_B\_20141006-L3.qps

Sample Desc: Comment:

Sample weight: 0.0514 g Sample Volume: 0.02151 cc

Outgas Time: 0.0 hrs OutgasTemp: 0.0 C

Analysis gas: Nitrogen Bath Temp: 77.3 K

Press. Tolerance:0.100/0.100 (ads/des)Equil time: 60/60 sec (ads/des) Equil timeout: 240/240 sec (ads/des)

Analysis Time: 405.7 min End of run: 2014/10/07 15:29:47 Instrument: Nova Station B

Cell ID: 4 F/W version: 0.00

Adsorbate Nitrogen Temperature 77.350K

 Molec. Wt.: 28.013 g Cross Section: 16.200 Ų Liquid Density: 0.808 g/cc

 Surface Area Data

MultiPoint BET 2.212e+00 m?g

Langmuir surface area 2.092e+00 m?g

BJH method cumulative adsorption surface area 8.453e+00 m?g

BJH method cumulative desorption surface area 1.037e+01 m?g

DH method cumulative adsorption surface area 1.005e+01 m?g

DH method cumulative desorption surface area 1.053e+01 m?g

t-method external surface area 2.212e+00 m?g

 Pore Volume Data

Total pore volume for pores with Diameter

less than 116.89 nm at P/Po = 0.983284 1.329e-02 cc/g

BJH method cumulative adsorption pore volume 1.589e-02 cc/g

BJH method cumulative desorption pore volume 1.542e-02 cc/g

DH method cumulative adsorption pore volume 1.591e-02 cc/g

DH method cumulative desorption pore volume 1.509e-02 cc/g

HK method cumulative pore volume 5.575e-04 cc/g

SF method cumulative pore volume 2.745e-05 cc/g

 Pore Size Data

Average pore Diameter 2.404e+01 nm

BJH method adsorption pore Diameter (Mode Dv(d)) 3.185e+00 nm

BJH method desorption pore Diameter (Mode Dv(d)) 2.432e+00 nm

DH method adsorption pore Diameter (Mode Dv(d)) 3.185e+00 nm

DH method desorption pore Diameter (Mode Dv(d)) 2.432e+00 nm

HK method pore Diameter (Mode) 1.337e+00 nm

SF method pore Diameter (Mode) 3.239e+00 nm

 Quantachrome NovaWin - Data Acquisition and Reduction

 for NOVA instruments

 ?1994-2010, Quantachrome Instruments

 version 11.0

Analysis Report

Operator:open Date:2014/10/07 Operator:open Date:10/7/2014

Sample ID: L3 Filename: C:\QCdata\Physisorb\sttn\_B\_20141006-L3.qps

Sample Desc: Comment:

Sample weight: 0.0514 g Sample Volume: 0.02151 cc

Outgas Time: 0.0 hrs OutgasTemp: 0.0 C

Analysis gas: Nitrogen Bath Temp: 77.3 K

Press. Tolerance:0.100/0.100 (ads/des)Equil time: 60/60 sec (ads/des) Equil timeout: 240/240 sec (ads/des)

Analysis Time: 405.7 min End of run: 2014/10/07 15:29:47 Instrument: Nova Station B

Cell ID: 4 F/W version: 0.00

Adsorbate Nitrogen Temperature 77.350K

 Molec. Wt.: 28.013 g Cross Section: 16.200 Ų Liquid Density: 0.808 g/cc

 Average Pore Size summary

 Average pore Diameter = 2.40380e+01 nm

 Quantachrome NovaWin - Data Acquisition and Reduction

 for NOVA instruments

 ?1994-2010, Quantachrome Instruments

 version 11.0

Analysis Report

Operator:open Date:2014/10/07 Operator:open Date:10/7/2014

Sample ID: L3 Filename: C:\QCdata\Physisorb\sttn\_B\_20141006-L3.qps

Sample Desc: Comment:

Sample weight: 0.0514 g Sample Volume: 0.02151 cc

Outgas Time: 0.0 hrs OutgasTemp: 0.0 C

Analysis gas: Nitrogen Bath Temp: 77.3 K

Press. Tolerance:0.100/0.100 (ads/des)Equil time: 60/60 sec (ads/des) Equil timeout: 240/240 sec (ads/des)

Analysis Time: 405.7 min End of run: 2014/10/07 15:29:47 Instrument: Nova Station B

Cell ID: 4 F/W version: 0.00

Adsorbate Nitrogen Temperature 77.350K

 Molec. Wt.: 28.013 g Cross Section: 16.200 Ų Liquid Density: 0.808 g/cc

 Relative Volume @ STP

 Pressure

 cc/g

 7.99600e-03 0.1347

 1.43440e-02 0.1964

 2.47290e-02 0.2698

 3.44360e-02 0.3164

 4.50430e-02 0.3267

 5.46500e-02 0.3340

 1.04108e-01 0.3473

 1.57733e-01 0.3665

 2.07306e-01 0.4878

 2.30502e-01 0.5605

 2.55285e-01 0.6703

 2.82833e-01 0.7763

 3.09088e-01 0.9007

 3.30812e-01 0.9904

 3.55872e-01 1.1233

 3.82743e-01 1.2554

 4.06832e-01 1.3961

 4.57815e-01 1.7037

 5.06780e-01 2.0268

 5.56992e-01 2.3516

 6.04694e-01 2.6981

 6.57618e-01 3.1128

 7.08755e-01 3.5529

 7.53283e-01 3.9904

 7.99659e-01 4.4522

 8.56235e-01 5.0731

 9.04491e-01 5.7259

 9.54834e-01 6.8721

 9.83284e-01 8.5949

 9.48148e-01 7.1996

 8.99945e-01 6.2646

 8.47221e-01 5.6329

 7.97926e-01 5.1514

 7.50779e-01 4.7439

 6.99881e-01 4.3307

 6.45308e-01 3.9247

 6.00064e-01 3.5811

 5.79780e-01 3.4757

 5.54227e-01 3.3144

 5.24529e-01 3.1342

 4.98121e-01 2.9730

 4.74894e-01 2.8280

 4.45844e-01 2.6328

 4.25860e-01 2.5235

 3.93358e-01 1.3092

 3.47806e-01 1.1015

 2.96623e-01 0.8124

 2.46418e-01 0.6407

 2.02176e-01 0.4806

 1.48273e-01 0.3733

 9.59960e-02 0.3551

 6.67450e-02 0.3404

 5.36250e-02 0.3304

 3.49750e-02 0.3223 Quantachrome NovaWin - Data Acquisition and Reduction

 for NOVA instruments

 ?1994-2010, Quantachrome Instruments

 version 11.0

Analysis Report

Operator:open Date:2014/10/07 Operator:open Date:10/7/2014

Sample ID: L3 Filename: C:\QCdata\Physisorb\sttn\_B\_20141006-L3.qps

Sample Desc: Comment:

Sample weight: 0.0514 g Sample Volume: 0.02151 cc

Outgas Time: 0.0 hrs OutgasTemp: 0.0 C

Analysis gas: Nitrogen Bath Temp: 77.3 K

Press. Tolerance:0.100/0.100 (ads/des)Equil time: 60/60 sec (ads/des) Equil timeout: 240/240 sec (ads/des)

Analysis Time: 405.7 min End of run: 2014/10/07 15:29:47 Instrument: Nova Station B

Cell ID: 4 F/W version: 0.00

Adsorbate Nitrogen Temperature 77.350K

 Molec. Wt.: 28.013 g Cross Section: 16.200 Ų Liquid Density: 0.808 g/cc

 Total Pore Volume summary

 Total Pore Volume

 Total pore volume = 1.329e-02 cc/g

 for pores smaller than 116.9 nm (Diameter)

 at P/Po = 0.98328