Supporting Information

Table of Content

Figure S1. Structure of AQ-[Zn]-AQ.	1

Figure S2. Image of the optimized structure ofAQ-[Zn]-AQ.	1

Figure S3. Representations of the frontier MOs of AQ-[Zn]-AQ.The MO energies are inHartree.	2

Table S1. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the AQ-[Zn]-AQ.	3

Figure S4. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for AQ-[Zn]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	5

Table S2. Atomic contributions for the frontier MO for AQ-[Zn]-AQ.	5

Figure S5. Structure of AQ-[S]-[Zn]-[S]-AQ.	6

Figure S6. Image of the optimized structure ofAQ-[S]-[Zn]-[S]-AQ.	6

Figure S7. Representations of the frontier MOs of AQ-[S]-[Zn]-[S]-AQ.The MOenergies are in Hartree.	7

Table S3. Computed positions of the electronic transitions, oscillator strength (f), andmajor contributions of the AQ-[S]-[Zn]-[S]-AQ.	8

Figure S8. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) forAQ-[S]-[Zn]-[S]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	10

Table S4. Atomic contributions for the frontier MO forAQ-[S]-[Zn]-[S]-AQ.	11

Figure S9. Structure of AQ-[B-Zn]-AQ.	11

Figure S10. Image of the optimized structure ofAQ-[B-Zn]-AQ.	11

Figure S11. Representations of the frontier MOs of AQ-[B-Zn]-AQ.The MO energies are inHartree.	12

Table S5. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the AQ-[B-Zn]-AQ.	13

Figure S12. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for AQ-[B-Zn]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	15

Table S6. Atomic contributions for the frontier MO for AQ-[B-Zn]-AQ.	15

Figure S13. Structure of AQ-[S]-[B-Zn]-[S]-AQ.	16

Figure S14. Image of the optimized structure ofAQ-[S]-[B-Zn]-[S]-AQ.	16

Figure S15. Representations of the frontier MOs of AQ-[S]-[B-Zn]-[S]-AQ.The MO energies arein Hartree.	17

Table S7. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the AQ-[S]-[B-Zn]-[S]-AQ.	18

Figure S16. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for AQ-[S]-[B-Zn]-[S]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	20

Table S8. Atomic contributions for the frontier MO for AQ-[S]-[B-Zn]-[S]-AQ.	20

Figure S17. Structure of NQ-[Zn]-NQ.	21

Figure S18. Image of the optimized structure ofNQ-[Zn]-NQ.	21

Figure S19. Representations of the frontier MOs ofNQ-[Zn]-NQ.The MO energies are in Hartree.	22

Table S9. Computed positions of the electronic transitions, oscillator strength (f), andmajor contributions of the NQ-[Zn]-NQ.	23

Figure S20. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[Zn]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	25

Table S10. Atomic contributions for the frontier MO for NQ-[Zn]-NQ.	25

Figure S21. Structure of NQ-[S]-[Zn]-[S]-NQ.	26

Figure S22. Image of the optimized structure ofNQ-[S]-[Zn]-[S]-NQ.	26

Figure S23. Representations of the frontier MOs ofNQ-[S]-[Zn]-[S]-NQ.The MO energies are in Hartree.	27

Table S11. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the NQ-[S]-[Zn]-[S]-NQ.	28

Figure S24. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[S]-[Zn]-[S]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	31

Table S12. Atomic contributions for the frontier MO for NQ-[S]-[Zn]-[S]-NQ.	31

Figure S26. Image of the optimized structure of NQ-[B-Zn]-NQ.	32

Figure S27. Representations of the frontier MOs of NQ-[B-Zn]-NQ.The MO energies are inHartree.	33

Table S13. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the NQ-[B-Zn]-NQ.	34

Figure S28. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[B-Zn]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	36

Table S14. Atomic contributions for the frontier MO for NQ-[B-Zn]-NQ.	36

Figure S29. Structure of NQ-[S]-[B-Zn]-[S]-NQ.	37

Figure S30. Image of the optimized structure of NQ-[S]-[B-Zn]-[S]-NQ.	37

Figure S31. Representations of the frontier MOs of NQ-[S]-[B-Zn]-[S]-NQ.The MO energies are in Hartree.	38

Table S15. Computed positions of the electronic transitions,oscillator strength (f), and major contributions of the NQ-[S]-[B-Zn]-[S]-NQ.	39

Figure S32. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[S]-[B-Zn]-[S]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	41

Table S16. Atomic contributions for the frontier MO for NQ-[S]-[B-Zn]-[S]-NQ.	42

Figure S33. Structure of ID-[Zn]-ID.	42

Figure S34. Image of the optimized structure of ID-[Zn]-ID.	42

Figure S35. Representations of the frontier MOs ofID-[Zn]-ID.The MO energies are in Hartree.	43

Table S17. Computed positions of the electronic transitions, oscillator strength (f), andmajor contributions of the ID-[Zn]-ID.	44

Figure S36. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for ID-[Zn]-ID.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	46

Table S18. Atomic contributions for the frontier MO for ID-[Zn]-ID.	47

Figure S37. Structure of NQ-[S]-[Zn]-[S]-NQ.	47

Figure S38. Image of the optimized structure of NQ-[S]-[Zn]-[S]-NQ.	47

Figure S39. Representations of the frontier MOs of NQ-[S]-[Zn]-[S]-NQ.The MO energies are inHartree.	48

Table S19. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the NQ-[S]-[Zn]-[S]-NQ.	49

Figure S40. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[S]-[Zn]-[S]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	51

Table S20. Atomic contributions for the frontier MO for NQ-[S]-[Zn]-[S]-NQ.	52

Figure S41. Structure of ID-[B-Zn]-ID.	52

Figure S42. Image of the optimized structure of ID-[B-Zn]-ID.	52

Figure S43. Representations of the frontier MOs of ID-[B-Zn]-ID.The MO energies are in Hartree.	53

Table S21. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the ID-[B-Zn]-ID.	54

Figure S44. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for ID-[B-Zn]-ID.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	56

Table S22. Atomic contributions for the frontier MO for ID-[B-Zn]-ID.	57

Figure S45. Structure of ID-[S]-[B-Zn]-[S]-ID.	57

Figure S46. Image of the optimized structure of ID-[S]-[B-Zn]-[S]-ID.	57

Figure S47. Representations of the frontier MOs ofID-[S]-[B-Zn]-[S]-ID.The MO energies are in Hartree.	58

Table S23. Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the ID-[S]-[B-Zn]-[S]-ID.	59

Figure S48. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for ID-[S]-[B-Zn]-[S]-ID.The black line represents a spectrum where 1000 cm-1 is applied to each transition.	61

Table S24. Atomic contributions for the frontier MO for ID-[S]-[B-Zn]-[S]-ID.	62

AQ-[Zn]-AQ

Figure S1. Structure of AQ-[Zn]-AQ.

Figure S2. Image of the optimized structure ofAQ-[Zn]-AQ.

H-4   (-0.23267)

H-3  (-0.22432)

H-2  (-0.22301)

H-1  (-0.20337)

HOMO  (-0.19115)

LUMO  (-0.11610)

L+1  (-0.10836)

L+2  (-0.09850)

L+3 (-0.09040)

L+4  (-0.06644)

Figure S3.Representations of the frontier MOs of AQ-[Zn]-AQ.The MO energies are inHartree.

Table S1.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the AQ-[Zn]-AQ.

| Wavelength (nm) | Oscillator strength (f) | Major contributions (%) |
| --- | --- | --- |
| 701.3 | 1.2960 | HOMO→LUMO (96) |
| 622.9 | 0.0000 | HOMO→L+1 (99) |
| 612.6 | 0.0161 | H-1→LUMO (71), HOMO→L+3 (27) |
| 563.6 | 0.0257 | H-1→L+3 (12), HOMO→L+2 (87) |
| 538.5 | 0.0000 | H-1→L+1 (100) |
| 521.1 | 0.0812 | H-1→LUMO (22), H-1→L+2 (46), HOMO→L+3 (32) |
| 479.0 | 0.0002 | H-2→LUMO (97) |
| 473.9 | 0.0851 | H-3→LUMO (93) |
| 439.1 | 0.0001 | H-4→LUMO (91) |
| 437.4 | 1.7666 | H-1→L+3 (48) |
| 437.0 | 1.2332 | H-1→L+2 (34), H-1→L+3 (18), HOMO→L+3 (27) |
| 430.0 | 0.0170 | H-2→L+1 (96) |
| 425.9 | 0.0000 | H-5→LUMO (88) |
| 425.2 | 0.0000 | H-3→L+1 (91) |
| 422.8 | 0.0714 | H-6→LUMO (84) |
| 419.5 | 0.0001 | H-13→L+1 (39), H-12→LUMO (36), H-12→L+2 (10) |
| 419.5 | 0.0000 | H-13→LUMO (36), H-13→L+2 (11), H-12→L+1 (39) |
| 409.2 | 0.0044 | H-7→LUMO (80), H-7→L+2 (16) |
| 405.2 | 0.0001 | HOMO→L+4 (91) |
| 403.8 | 0.0116 | H-4→L+1 (70) |
| 402.1 | 0.0002 | H-2→L+2 (95) |
| 397.0 | 0.0520 | H-3→L+2 (84) |
| 396.9 | 0.0002 | H-2→L+3 (91) |
| 392.0 | 0.1201 | H-3→L+3 (78) |
| 387.4 | 0.0000 | H-9→LUMO (68), H-6→L+1 (17) |
| 386.7 | 0.0006 | H-5→L+1 (79) |
| 386.3 | 0.0227 | H-8→LUMO (80) |
| 385.7 | 0.0000 | H-9→LUMO (15), H-6→L+1 (66), H-4→L+2 (11) |
| 383.8 | 0.0000 | H-22→L+1 (36), H-21→LUMO (31), H-21→L+2 (11) |
| 383.8 | 0.0000 | H-22→LUMO (31), H-22→L+2 (11), H-21→L+1 (36) |
| 378.4 | 0.0000 | H-10→LUMO (19), H-6→L+1 (14), H-4→L+2 (52) |
| 378.3 | 0.0144 | HOMO→L+5 (71) |
| 369.6 | 0.0001 | H-10→LUMO (61), H-4→L+2 (27) |
| 366.5 | 0.0000 | H-4→L+3 (45), H-1→L+4 (46) |
| 364.1 | 0.0000 | H-5→L+2 (62), H-1→L+4 (20) |
| 362.6 | 0.0001 | H-5→L+2 (19), H-5→L+3 (17), H-4→L+3 (37), H-1→L+4 (21) |
| 362.4 | 0.0129 | H-6→L+2 (94) |
| 359.3 | 0.0643 | H-6→L+3 (82) |
| 359.0 | 0.0002 | H-5→L+3 (76), H-1→L+4 (11) |
| 356.3 | 0.0014 | H-7→L+3 (94) |
| 351.8 | 0.0000 | H-14→LUMO (34), H-11→LUMO (29) |
| 349.3 | 0.0000 | H-7→L+1 (99) |
| 345.9 | 0.1954 | H-14→LUMO (42), H-11→LUMO (28) |
| 345.8 | 0.0000 | HOMO→L+6 (79) |
| 344.9 | 0.0837 | H-1→L+5 (94) |
| 344.9 | 0.0000 | H-8→L+1 (93) |
| 342.9 | 0.0038 | H-9→L+1 (89) |
| 338.5 | 0.0000 | H-20→L+1 (13), H-19→LUMO (24), H-11→L+1 (34) |
| 337.0 | 0.0015 | H-7→LUMO (17), H-7→L+2 (81) |
| 334.3 | 0.0205 | H-10→L+1 (70) |
| 334.0 | 0.1204 | H-20→LUMO (16), H-16→LUMO (42), H-15→L+1 (22) |
| 333.8 | 0.0000 | H-16→L+1 (26), H-15→LUMO (53) |
| 331.3 | 0.0037 | H-20→LUMO (24), H-19→L+1 (11), H-16→LUMO (17), H-10→L+1 (12) |
| 328.6 | 0.0043 | H-8→L+2 (83) |
| 328.0 | 0.0000 | H-19→LUMO (12), H-11→L+1 (21), H-9→L+3 (13) |
| 327.9 | 0.0157 | H-8→L+3 (90) |
| 327.5 | 0.0000 | H-9→L+2 (71) |
| 326.1 | 0.0000 | H-25→LUMO (17), H-13→L+1 (13), H-12→LUMO (43), H-12→L+2 (14) |
| 326.0 | 0.0000 | H-27→LUMO (16), H-13→LUMO (44), H-13→L+2 (14), H-12→L+1 (14) |
| 325.2 | 0.0000 | H-11→L+1 (19), H-9→L+3 (62) |
| 319.1 | 0.0000 | H-10→L+2 (11), H-10→L+3 (47), H-1→L+6 (28) |
| 319.0 | 0.0003 | H-18→LUMO (83) |
| 318.9 | 0.0000 | H-17→LUMO (86) |
| 318.4 | 0.0000 | H-14→L+1 (16), H-10→L+2 (44), H-10→L+3 (10), H-9→L+3 (13) |
| 315.4 | 0.0000 | H-27→LUMO (58), H-13→LUMO (12), H-12→L+1 (11) |
| 315.3 | 0.0001 | H-25→LUMO (56), H-13→L+1 (10), H-12→LUMO (12) |
| 313.9 | 0.0155 | H-24→LUMO (15), H-11→L+2 (44), HOMO→L+7 (21) |
| 312.4 | 0.0001 | H-10→L+3 (34), H-1→L+6 (54) |
| 311.0 | 0.0099 | H-2→L+4 (96) |
| 311.0 | 0.0000 | H-14→L+1 (78), H-10→L+2 (16) |
| 308.7 | 0.0001 | H-3→L+4 (91) |
| 306.6 | 0.0000 | H-23→LUMO (53), H-19→LUMO (12) |
| 304.9 | 0.0001 | H-16→LUMO (33), H-16→L+2 (11), H-15→L+1 (47) |
| 304.8 | 0.0000 | H-16→L+1 (47), H-15→LUMO (32), H-15→L+2 (10) |
| 303.6 | 0.0570 | H-24→LUMO (21), H-20→LUMO (12), H-11→L+2 (39), HOMO→L+7 (14) |
| 301.2 | 0.1327 | H-24→LUMO (25), H-14→L+2 (17), HOMO→L+7 (43) |
| 299.7 | 0.0019 | H-21→LUMO (34), H-13→L+1 (15), H-12→L+2 (18) |
| 299.7 | 0.0000 | H-22→LUMO (36), H-22→L+2 (10), H-13→L+2 (18), H-12→L+1 (16) |
| 299.6 | 0.0316 | H-20→LUMO (28), H-20→L+2 (10), H-19→L+1 (40) |
| 299.3 | 0.0461 | H-14→L+2 (60), H-14→L+3 (10), HOMO→L+7 (10) |
| 299.3 | 0.0000 | H-20→L+1 (41), H-19→LUMO (26), H-19→L+2 (10) |
| 298.8 | 0.0168 | H-14→L+2 (10), H-14→L+3 (79) |
| 298.4 | 0.0003 | H-17→L+1 (94) |
| 298.3 | 0.0000 | H-18→L+1 (92) |
| 296.8 | 0.0001 | H-2→L+5 (94) |
| 296.7 | 0.0000 | HOMO→L+8 (81) |
| 295.8 | 0.0003 | H-22→L+1 (14), H-21→LUMO (20), H-13→L+1 (13), H-12→L+2 (45) |
| 295.8 | 0.0000 | H-22→LUMO (20), H-21→L+1 (14), H-13→L+2 (45), H-12→L+1 (13) |
| 295.6 | 0.1634 | H-11→L+3 (14), H-4→L+4 (42), H-3→L+5 (31) |
| 294.1 | 0.0003 | H-26→LUMO (80) |
| 294.1 | 0.4587 | H-11→L+3 (64), H-4→L+4 (19) |
| 293.8 | 0.0507 | H-4→L+4 (22), H-3→L+5 (67) |
| 288.0 | 0.0424 | H-27→L+1 (16), H-25→L+2 (11), H-23→L+1 (38) |
| 287.8 | 0.0000 | H-27→L+2 (32), H-25→L+1 (52) |
| 287.7 | 0.0199 | H-27→L+1 (36), H-25→L+2 (24), H-23→L+1 (14) |
| 287.5 | 0.0174 | H-23→L+1 (11), H-5→L+4 (76) |
| 287.3 | 0.0002 | H-6→L+4 (75) |
| 285.9 | 0.0000 | H-24→L+1 (56), H-23→L+2 (10) |
| 284.0 | 0.0000 | H-16→L+1 (14), H-15→L+2 (67) |
| 283.8 | 0.0000 | H-28→LUMO (25), H-17→L+2 (66) |

Figure S4.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for AQ-[Zn]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S2.Atomic contributions for the frontier MO for AQ-[Zn]-AQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ethyne-porphyrins | 0.76 | 0.99 | 0.99 | ~1.00 | 0.88 | 0.40 | 0.05 | 0.48 | ~1.00 | 0.19 |
| 2*anthranquinone | 0.24 | 0.01 | 0.01 | ~0.0 | 0.12 | 0.60 | 0.95 | 0.52 | ~0.0 | 0.81 |

AQ-[S]-[Zn]-[S]-AQ

Figure S5.Structure of AQ-[S]-[Zn]-[S]-AQ.

Figure S6. Image of the optimized structure ofAQ-[S]-[Zn]-[S]-AQ.

H-4 (-0.21643)

H-3 (-0.21593)

H-2 (-0.20639)

H-1 (-0.19873)

HOMO (-0.17973)

LUMO (-0.10904)

L+1 (-0.10369)

L+2 (-0.09872)

L+3 (-0.08540)

.

L+4  (-0.07308)

Figure S7.Representations of the frontier MOs of AQ-[S]-[Zn]-[S]-AQ.The MOenergies are in Hartree.

Table S3. Computed positions of the electronic transitions, oscillator strength (f), andmajor contributions of the AQ-[S]-[Zn]-[S]-AQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 748.7 | 2.4636 | HOMO→LUMO (95%) |
| 661.8 | 0 | HOMO→L+1 (99%) |
| 622.8 | 0.0887 | HOMO→L+2 (94%) |
| 615.5 | 0.0007 | H-1→LUMO (43%), HOMO→L+3 (48%) |
| 524.9 | 0 | H-2→LUMO (95%) |
| 518.9 | 0.1474 | H-1→LUMO (50%), H-1→L+2 (-28%), HOMO→L+3 (-20%) |
| 517.2 | 0 | H-1→L+1 (99%) |
| 490.5 | 1.1445 | H-3→LUMO (-28%), H-2→L+1 (51%), H-1→L+3 (-12%) |
| 478.8 | 0.1642 | H-3→LUMO (38%), H-2→L+1 (34%), H-1→L+2 (-13%) |
| 476.2 | 0.0003 | H-4→LUMO (86%) |
| 473.0 | 0 | H-2→L+2 (13%), HOMO→L+4 (79%) |
| 467.9 | 0.9985 | H-5→LUMO (12%), H-1→L+2 (30%), H-1→L+3 (20%), HOMO→L+3 (-15%) |
| 462.4 | 0 | H-2→L+2 (79%), HOMO→L+4 (-14%) |
| 461.0 | 0.6798 | H-3→LUMO (-21%), H-1→L+2 (-16%), H-1→L+3 (23%), HOMO→L+3 (11%), HOMO→L+5 (10%) |
| 443.1 | 0.124 | H-5→LUMO (-43%), HOMO→L+5 (47%) |
| 431.0 | 0 | H-3→L+1 (94%) |
| 428.1 | 0.0001 | H-4→L+1 (98%) |
| 426.4 | 0 | H-6→LUMO (35%), H-2→L+3 (57%) |
| 421.8 | 0 | H-6→LUMO (54%), H-2→L+3 (-38%) |
| 420.9 | 0 | H-14→L+1 (30%), H-13→LUMO (20%), H-13→L+1 (16%), H-13→L+2 (-17%) |
| 420.9 | 0 | H-14→LUMO (20%), H-14→L+1 (-16%), H-14→L+2 (-17%), H-13→L+1 (30%) |
| 420.5 | 0.0049 | H-7→LUMO (12%), H-3→L+2 (49%), HOMO→L+5 (-14%) |
| 417.8 | 0.0029 | H-7→LUMO (42%), H-3→L+2 (-34%) |
| 416.6 | 0.0001 | H-4→L+2 (87%) |
| 411.1 | 0.0154 | H-8→LUMO (56%), H-8→L+2 (18%) |
| 407.8 | 0.0001 | H-5→L+1 (81%) |
| 406.2 | 0.0634 | H-8→LUMO (16%), H-7→LUMO (17%), H-3→L+3 (40%) |
| 403.0 | 0.0002 | H-4→L+3 (82%) |
| 399.6 | 0.0432 | H-5→L+2 (40%), H-3→L+3 (34%) |
| 396.5 | 0 | H-1→L+4 (91%) |
| 387.9 | 0.1611 | H-6→L+1 (-12%), H-5→L+2 (34%) |
| 385.2 | 0 | H-25→LUMO (23%), H-25→L+1 (43%), H-25→L+2 (-21%) |
| 385.2 | 0 | H-26→LUMO (-23%), H-26→L+1 (43%), H-26→L+2 (21%) |
| 384.2 | 0.0353 | H-6→L+1 (85%) |
| 382.3 | 0 | HOMO→L+6 (84%) |
| 381.5 | 0.0041 | H-10→LUMO (74%), H-10→L+2 (16%) |
| 380.7 | 0 | H-11→LUMO (23%), H-9→LUMO (45%) |
| 380.1 | 0 | H-11→LUMO (53%), H-11→L+2 (11%), H-9→LUMO (-24%) |
| 376.9 | 0 | H-7→L+1 (71%), H-6→L+2 (10%) |
| 374.8 | 0 | H-6→L+2 (79%) |
| 372.6 | 0.1681 | H-5→L+3 (45%), H-2→L+4 (15%), H-1→L+5 (19%) |
| 369.2 | 0.2148 | H-2→L+4 (53%), HOMO→L+7 (-24%) |
| 368.4 | 0.0368 | H-7→L+2 (74%), HOMO→L+7 (12%) |
| 366.5 | 0.2151 | H-7→L+3 (18%), H-1→L+5 (59%), HOMO→L+7 (-10%) |
| 365.0 | 0.0003 | H-6→L+3 (94%) |
| 361.5 | 0.0052 | H-8→L+3 (92%) |
| 355.9 | 0.2504 | H-2→L+4 (14%), HOMO→L+7 (37%) |
| 350.4 | 0 | H-3→L+4 (-11%), H-2→L+5 (66%) |
| 346.3 | 0 | H-20→L+1 (-12%), H-12→LUMO (30%), H-9→L+2 (-12%), H-8→L+1 (11%) |
| 346.3 | 0.0077 | H-9→L+1 (69%) |
| 344.5 | 0.2127 | H-7→L+3 (60%), H-5→L+3 (17%) |
| 344.2 | 0 | H-8→L+1 (87%) |
| 342.0 | 0.0455 | H-15→LUMO (50%), H-15→L+2 (10%) |
| 340.3 | 0 | H-3→L+4 (43%), H-2→L+5 (14%), HOMO→L+8 (31%) |
| 339.1 | 0.0072 | H-8→LUMO (-22%), H-8→L+2 (68%) |
| 339.0 | 0.0043 | H-4→L+4 (94%) |
| 338.8 | 0 | H-9→L+2 (-10%), H-3→L+4 (40%), HOMO→L+8 (-39%) |
| 336.6 | 0 | H-10→L+1 (93%) |
| 335.2 | 0.0058 | H-11→L+1 (84%), H-10→L+2 (10%) |
| 334.7 | 0.1054 | H-24→LUMO (-10%), H-21→L+1 (22%), H-20→LUMO (13%), H-9→L+1 (15%) |
| 332.8 | 0 | H-24→L+1 (-11%), H-21→LUMO (16%), H-18→L+1 (13%), H-9→L+2 (-12%) |
| 331.6 | 0.0783 | H-19→L+1 (38%), H-18→LUMO (-37%), H-18→L+2 (12%) |
| 331.6 | 0 | H-19→LUMO (-16%), H-18→L+1 (14%), H-12→LUMO (15%), H-9→L+2 (33%) |
| 331.0 | 0 | H-11→LUMO (-11%), H-11→L+2 (24%), H-9→L+3 (44%) |
| 329.9 | 0 | H-19→LUMO (13%), H-12→LUMO (22%) |
| 329.6 | 0.0085 | H-11→L+1 (-10%), H-10→LUMO (-16%), H-10→L+2 (71%) |
| 328.7 | 0 | H-11→L+2 (13%), H-1→L+6 (77%) |
| 327.5 | 0.0125 | H-15→LUMO (-11%), H-10→L+3 (80%) |
| 326.6 | 0 | H-11→L+2 (-39%), H-9→L+3 (41%) |
| 324.9 | 0.0069 | H-24→LUMO (-10%), H-12→L+1 (26%), H-3→L+5 (-12%), H-2→L+6 (13%) |
| 324.6 | 0 | H-11→L+3 (75%), H-5→L+4 (-12%) |
| 323.1 | 0 | H-11→L+3 (13%), H-5→L+4 (68%) |
| 320.9 | 0 | H-17→LUMO (35%), H-14→LUMO (11%), H-13→LUMO (-28%) |
| 320.8 | 0 | H-16→LUMO (-13%), H-14→LUMO (42%), H-14→L+2 (10%), H-13→LUMO (16%) |
| 320.6 | 0 | H-16→LUMO (63%), H-13→LUMO (14%) |
| 320.6 | 0 | H-17→LUMO (42%), H-16→LUMO (-16%), H-14→LUMO (-14%), H-13→LUMO (10%) |
| 319.6 | 0.1031 | H-3→L+5 (82%) |
| 318.7 | 0.0001 | H-4→L+5 (95%) |
| 317.0 | 0 | H-27→LUMO (-10%), H-20→L+1 (10%), H-12→L+2 (38%) |
| 315.8 | 0.0602 | H-1→L+7 (93%) |
| 314.2 | 0.0315 | H-22→LUMO (77%) |
| 313.5 | 0 | H-23→LUMO (75%) |
| 313.2 | 0.0003 | H-20→LUMO (33%), H-12→L+1 (35%), H-2→L+6 (-13%) |
| 311.3 | 0.007 | H-6→L+4 (95%) |
| 310.1 | 0.0001 | H-29→LUMO (66%) |
| 310.1 | 0 | H-30→LUMO (60%) |
| 309.7 | 0.0558 | H-24→LUMO (16%), H-2→L+6 (58%) |
| 306.7 | 0 | H-15→L+1 (94%) |
| 306.2 | 0.23 | H-5→L+5 (75%) |
| 306.0 | 0 | H-7→L+4 (93%) |
| 303.6 | 0.012 | H-19→L+1 (21%), H-18→LUMO (44%), H-18→L+2 (11%) |
| 303.5 | 0 | H-19→LUMO (55%), H-19→L+2 (15%), H-18→L+1 (22%) |
| 302.9 | 0 | H-12→L+2 (32%), H-2→L+7 (20%) |
| 302.7 | 0.0522 | H-28→LUMO (19%), H-27→L+1 (11%), H-5→L+5 (12%), HOMO→L+9 (-13%) |
| 302.6 | 0 | H-14→L+1 (27%), H-14→L+2 (-12%), H-13→L+1 (13%), H-13→L+2 (31%) |
| 302.6 | 0 | H-14→L+1 (-13%), H-14→L+2 (31%), H-13→L+1 (26%), H-13→L+2 (11%) |
| 301.3 | 0.0322 | H-15→LUMO (-14%), H-15→L+2 (74%) |
| 301.1 | 0.0016 | H-17→L+1 (31%), H-16→L+1 (62%) |
| 301.1 | 0.001 | H-17→L+1 (60%), H-16→L+1 (-33%) |

Figure S8.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) forAQ-[S]-[Zn]-[S]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S4.Atomic contributions for the frontier MO forAQ-[S]-[Zn]-[S]-AQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2*thiophene-porphyrins | ~1.00 | 0.96 | 0.86 | ~1.00 | 0.96 | 0.60 | 0.09 | 0.43 | ~1.00 | 0.61 |
| anthranquinone | ~0.0 | 0 04 | 0.14 | ~0.0 | 0.04 | 0.40 | 0.91 | 0.57 | ~0.0 | 0.39 |

AQ-[B-Zn]-AQ

Figure S9.Structure of AQ-[B-Zn]-AQ.

Figure S10. Image of the optimized structure ofAQ-[B-Zn]-AQ.

H-4   (-0.21947)

H-3  (-0.21622)

H-2  (-0.21491)

H-1  (-0.18536)

HOMO  (-0.17511)

LUMO  (-0.10783)

L+1  (-0.10160)

L+2  (-0.09095)

L+3 (-0.08292)

L+4  (-0.06099)

Figure S11.Representations of the frontier MOs of AQ-[B-Zn]-AQ.The MO energies are inHartree.

Table S5.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the AQ-[B-Zn]-AQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 794.3 | 0.1243 | HOMO→LUMO (96%) |
| 723.1 | 0.0008 | HOMO→L+1 (100%) |
| 700.4 | 0.7058 | H-1→LUMO (84%), HOMO→L+3 (13%) |
| 633.4 | 0.0962 | H-1→L+3 (13%), HOMO→L+2 (86%) |
| 618.3 | 0.0003 | H-1→L+1 (99%) |
| 593.3 | 0.4669 | H-1→LUMO (13%), H-1→L+2 (44%), HOMO→L+3 (-43%) |
| 501.2 | 2.0363 | H-1→L+2 (53%), HOMO→L+3 (41%) |
| 483.7 | 0.9802 | H-1→L+3 (77%), HOMO→L+2 (-14%) |
| 478.9 | 0.0011 | H-2→LUMO (95%) |
| 471.3 | 0.0734 | H-3→LUMO (92%) |
| 460.8 | 0.0001 | H-4→LUMO (94%) |
| 447.5 | 0.012 | HOMO→L+4 (98%) |
| 438.0 | 0.0034 | H-2→L+1 (90%) |
| 430.8 | 0.0004 | H-3→L+1 (95%) |
| 427.0 | 0.0085 | H-6→LUMO (-14%), H-4→L+1 (71%) |
| 423.2 | 0.0033 | H-5→LUMO (89%) |
| 421.1 | 0.0001 | H-15→LUMO (31%), H-14→L+1 (34%), H-6→LUMO (19%) |
| 420.9 | 0 | H-15→L+1 (43%), H-14→LUMO (40%), H-14→L+2 (10%) |
| 420.1 | 0.0016 | H-14→L+1 (-10%), H-6→LUMO (59%), H-4→L+1 (13%) |
| 417.0 | 0.1747 | HOMO→L+5 (95%) |
| 410.2 | 0.0007 | H-2→L+2 (10%), H-1→L+4 (83%) |
| 407.2 | 0.0004 | H-2→L+2 (79%), H-1→L+4 (-11%) |
| 405.4 | 0.0002 | H-7→LUMO (76%) |
| 401.9 | 0.0068 | H-3→L+2 (93%) |
| 397.3 | 0.0033 | H-4→L+2 (28%), H-2→L+3 (60%) |
| 394.9 | 0.0015 | H-4→L+2 (50%), H-2→L+3 (-32%) |
| 392.6 | 0.0003 | H-9→LUMO (12%), H-8→LUMO (-14%), H-3→L+3 (65%) |
| 391.6 | 0 | H-9→LUMO (-30%), H-8→LUMO (28%), H-3→L+3 (31%) |
| 389.9 | 0.0052 | H-5→L+1 (88%) |
| 387.7 | 0.0003 | H-6→L+1 (85%) |
| 386.0 | 0 | H-10→LUMO (69%) |
| 385.5 | 0.0031 | H-25→LUMO (19%), H-24→L+1 (20%), H-9→LUMO (15%), H-8→LUMO (12%), H-1→L+5 (-16%) |
| 384.9 | 0 | H-25→L+1 (35%), H-24→LUMO (26%), H-10→LUMO (13%) |
| 384.9 | 0.0097 | H-25→LUMO (17%), H-24→L+1 (16%), H-1→L+5 (31%) |
| 382.2 | 0.0353 | H-9→LUMO (20%), H-8→LUMO (20%), H-1→L+5 (39%) |
| 381.9 | 0.0015 | H-4→L+3 (75%), HOMO→L+6 (-14%) |
| 377.6 | 0.0044 | H-11→LUMO (49%), HOMO→L+6 (38%) |
| 373.8 | 0.0264 | H-13→LUMO (72%), H-13→L+2 (-16%) |
| 372.7 | 0.0571 | H-11→LUMO (-32%), HOMO→L+6 (38%) |
| 369.1 | 0.037 | H-12→LUMO (30%), H-7→L+1 (54%) |
| 368.1 | 0.0548 | H-12→LUMO (43%), H-7→L+1 (-40%) |
| 365.6 | 0.0147 | H-5→L+2 (86%) |
| 365.0 | 0.0046 | H-6→L+2 (92%) |
| 358.2 | 0.0003 | H-8→L+1 (27%), H-5→L+3 (58%) |
| 357.8 | 0.0137 | H-6→L+3 (95%) |
| 357.3 | 0.0005 | H-8→L+1 (48%), H-5→L+3 (-28%) |
| 356.1 | 0.0016 | H-9→L+1 (72%) |
| 354.2 | 0 | H-1→L+6 (36%), HOMO→L+8 (49%) |
| 351.8 | 0.0143 | H-10→L+1 (77%) |
| 348.0 | 0.0094 | H-7→L+2 (71%) |
| 347.3 | 0.0066 | H-11→L+1 (78%), H-9→L+2 (12%) |
| 346.0 | 0.0001 | H-1→L+6 (44%), HOMO→L+8 (-32%) |
| 343.3 | 0.0013 | H-17→LUMO (46%), H-16→L+1 (14%) |
| 342.9 | 0 | H-17→L+1 (15%), H-16→LUMO (52%) |
| 342.2 | 0.0111 | HOMO→L+7 (89%) |
| 341.8 | 0 | H-12→L+1 (27%), H-10→L+2 (32%), H-7→L+3 (26%) |
| 337.7 | 0.0011 | H-10→L+3 (11%), H-1→L+8 (-10%), HOMO→L+9 (69%) |
| 337.4 | 0.005 | H-11→L+1 (13%), H-9→L+2 (-20%), H-8→L+2 (49%) |
| 336.9 | 0.0002 | H-12→L+1 (48%), H-7→L+3 (-34%) |
| 336.4 | 0.0063 | H-9→L+2 (52%), H-8→L+2 (24%) |
| 334.8 | 0.0444 | H-9→L+3 (-30%), H-8→L+3 (37%) |
| 332.9 | 0.0344 | H-13→L+3 (81%) |
| 332.1 | 0.0003 | H-22→LUMO (-20%), H-18→LUMO (-14%), H-13→L+1 (29%) |
| 331.7 | 0.1556 | H-23→LUMO (12%), H-19→LUMO (41%), H-18→L+1 (25%) |
| 331.3 | 0.0003 | H-19→L+1 (15%), H-18→LUMO (26%), H-13→L+1 (36%) |
| 330.6 | 0.0065 | H-11→L+2 (43%), H-10→L+3 (34%), HOMO→L+9 (-10%) |
| 330.3 | 0.0002 | H-13→L+1 (14%), H-12→L+1 (-16%), H-10→L+2 (32%) |
| 328.9 | 0.0247 | H-23→LUMO (19%), H-19→LUMO (-12%), H-17→LUMO (14%) |
| 328.8 | 0 | H-22→LUMO (13%), H-18→LUMO (-13%), H-16→LUMO (17%) |
| 326.7 | 0.0577 | H-11→L+2 (17%), H-1→L+8 (59%) |
| 326.2 | 0.0004 | H-26→LUMO (14%), H-14→LUMO (16%), H-13→L+1 (-13%), H-10→L+2 (12%) |
| 324.6 | 0.0012 | H-30→LUMO (16%), H-15→LUMO (-15%), HOMO→L+10 (21%) |
| 323.6 | 0.0132 | H-11→L+2 (-28%), H-10→L+3 (47%), H-1→L+8 (19%) |
| 323.1 | 0.0009 | HOMO→L+10 (61%) |
| 322.6 | 0.0049 | H-13→L+3 (-11%), H-9→L+3 (29%), H-8→L+3 (43%) |
| 320.5 | 0.0017 | H-12→L+2 (53%), H-1→L+7 (-18%) |
| 320.1 | 0.0006 | H-11→L+3 (63%), H-1→L+9 (-15%) |
| 319.5 | 0.0231 | H-15→LUMO (-11%), H-13→LUMO (10%), H-13→L+2 (54%) |
| 319.0 | 0.0914 | H-12→L+2 (26%), H-2→L+4 (-10%), H-1→L+7 (37%) |
| 318.6 | 0.0001 | H-26→LUMO (13%), H-17→L+1 (19%), H-16→LUMO (-11%), H-15→L+1 (15%), H-14→LUMO (-17%) |
| 317.9 | 0.0728 | H-2→L+4 (60%) |
| 317.0 | 0.0154 | H-20→LUMO (44%) |
| 316.5 | 0 | H-29→LUMO (12%), H-21→LUMO (11%), H-17→L+1 (20%), H-14→LUMO (14%) |
| 315.9 | 0.0411 | H-16→L+1 (20%), H-1→L+7 (18%) |
| 315.0 | 0.0001 | H-21→LUMO (78%) |
| 314.7 | 0.1035 | H-12→L+3 (87%) |
| 314.5 | 0 | H-3→L+4 (92%) |
| 313.3 | 0.0338 | HOMO→L+11 (83%) |
| 312.8 | 0.0285 | H-30→LUMO (-22%), H-20→LUMO (38%) |
| 312.2 | 0.0503 | HOMO→L+12 (85%) |
| 311.5 | 0.1595 | H-4→L+4 (64%) |
| 310.8 | 0.0003 | H-11→L+3 (16%), H-1→L+9 (66%) |
| 305.6 | 0.0059 | H-27→LUMO (86%) |
| 303.4 | 0.0001 | H-2→L+5 (79%) |
| 302.2 | 0.0917 | H-28→LUMO (-15%), H-1→L+10 (45%) |
| 302.0 | 0.0002 | H-29→LUMO (22%), H-19→L+1 (11%), H-17→L+1 (-14%) |
| 301.9 | 0.0089 | H-19→LUMO (-10%), H-18→L+1 (14%), H-1→L+10 (44%) |
| 301.7 | 0 | H-19→L+1 (37%), H-18→LUMO (-29%) |
| 301.6 | 0.0248 | H-28→LUMO (-14%), H-19→LUMO (-22%), H-18→L+1 (28%) |

Figure S12.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for AQ-[B-Zn]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S6.Atomic contributions for the frontier MO for AQ-[B-Zn]-AQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ethyne-benzo-porphyrins | ~1.00 | 0.96 | 0.86 | ~1.00 | 0.96 | 0.60 | 0.09 | 0.43 | ~1.00 | 0.61 |
| 2*anthranquinone | ~0.0 | 0 04 | 0.14 | ~0.0 | 0.04 | 0.40 | 0.91 | 0.57 | ~0.0 | 0.39 |

AQ-[S]-[B-Zn]-[S]-AQ

Figure S13.Structure of AQ-[S]-[B-Zn]-[S]-AQ.

Figure S14.Image of the optimized structure ofAQ-[S]-[B-Zn]-[S]-AQ.

H-4   (-0.21537)

H-3   (-0.21448)

H-2   (-0.20338)

H-1   (-0.18002)

HOMO   (-0.17506)

LUMO  (-0.10683)

L+1   (-0.10370)

L+2   (-0.09665)

L+3   (-0.08283)

L+4   (-0.07356)

Figure S15.Representations of the frontier MOs of AQ-[S]-[B-Zn]-[S]-AQ.The MO energies are in Hartree.

Table S7.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the AQ-[S]-[B-Zn]-[S]-AQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 763.9 | 0.1239 | HOMO→LUMO (89%) |
| 732.1 | 1.6409 | H-1→LUMO (84%) |
| 708.0 | 0.0004 | HOMO→L+1 (100%) |
| 663.3 | 0.0645 | H-1→L+3 (10%), HOMO→L+2 (81%) |
| 660.3 | 0.0002 | H-1→L+1 (99%) |
| 631.1 | 0.0821 | H-1→LUMO (13%), H-1→L+2 (64%), HOMO→L+3 (-22%) |
| 545.9 | 2.8724 | H-1→L+2 (26%), HOMO→L+3 (58%) |
| 529.3 | 0.0004 | H-2→LUMO (93%) |
| 515.2 | 0.6619 | H-1→L+3 (75%), HOMO→L+2 (-14%) |
| 503.7 | 0.007 | HOMO→L+4 (98%) |
| 496.6 | 0.0566 | H-2→L+1 (88%) |
| 476.7 | 0.0002 | H-1→L+4 (93%) |
| 471.8 | 0 | H-2→L+2 (86%) |
| 467.4 | 0.0063 | H-3→LUMO (81%), H-3→L+2 (-12%) |
| 465.4 | 0.0007 | H-4→LUMO (81%), H-4→L+2 (-15%) |
| 454.7 | 0.379 | HOMO→L+5 (89%) |
| 442.9 | 0.008 | H-5→LUMO (50%), H-1→L+5 (-39%) |
| 437.8 | 0.0001 | H-3→L+1 (94%) |
| 432.5 | 0.0025 | H-4→L+1 (98%) |
| 429.4 | 0.0046 | H-2→L+3 (85%) |
| 426.6 | 0.0461 | H-5→LUMO (20%), H-3→L+2 (28%), H-1→L+5 (34%) |
| 420.7 | 0 | H-17→L+1 (46%), H-16→LUMO (35%), H-16→L+2 (13%) |
| 420.7 | 0 | H-17→LUMO (35%), H-17→L+2 (13%), H-16→L+1 (46%) |
| 419.6 | 0.0111 | H-5→LUMO (-17%), H-3→L+2 (55%), H-1→L+5 (-13%) |
| 418.5 | 0.0012 | H-4→LUMO (13%), H-4→L+2 (76%) |
| 417.8 | 0.0058 | H-6→LUMO (69%), H-6→L+2 (-12%) |
| 413.9 | 0.001 | H-5→L+1 (76%) |
| 407.7 | 0.0353 | H-7→LUMO (70%), H-7→L+2 (-10%) |
| 398.0 | 0.0063 | H-8→LUMO (-19%), HOMO→L+6 (69%) |
| 397.5 | 0.0076 | H-5→L+2 (71%) |
| 396.3 | 0.0189 | H-8→LUMO (50%), H-8→L+2 (-14%), HOMO→L+6 (23%) |
| 395.8 | 0.0526 | H-3→L+3 (91%) |
| 395.0 | 0 | H-4→L+3 (93%) |
| 390.5 | 0.0031 | H-6→L+1 (93%) |
| 387.9 | 0 | H-9→LUMO (62%), H-7→L+1 (12%) |
| 385.1 | 0.0006 | H-10→LUMO (70%), H-10→L+2 (-23%) |
| 385.1 | 0 | H-28→LUMO (17%), H-28→L+1 (20%), H-27→LUMO (14%), H-27→L+1 (23%) |
| 385.1 | 0 | H-28→LUMO (-14%), H-28→L+1 (24%), H-27→LUMO (16%), H-27→L+1 (-19%) |
| 383.5 | 0 | H-7→L+1 (-22%), H-1→L+6 (57%) |
| 382.2 | 0.0875 | HOMO→L+7 (86%) |
| 382.1 | 0.0003 | H-7→L+1 (61%), H-1→L+6 (31%) |
| 381.9 | 0.5007 | H-2→L+4 (82%) |
| 379.3 | 0.0016 | H-6→LUMO (16%), H-6→L+2 (79%) |
| 372.8 | 0.0146 | H-7→LUMO (11%), H-7→L+2 (67%) |
| 370.2 | 0.0019 | H-12→LUMO (22%), H-11→LUMO (39%) |
| 369.9 | 0.0497 | H-15→LUMO (33%), H-15→L+2 (-22%), H-1→L+7 (-32%) |
| 368.7 | 0.0054 | H-12→LUMO (46%), H-12→L+2 (-12%), H-11→LUMO (-17%) |
| 367.8 | 0.1032 | H-8→L+1 (41%), H-5→L+3 (31%) |
| 366.7 | 0.0652 | H-13→LUMO (-15%), H-5→L+3 (32%), H-1→L+7 (-22%) |
| 366.3 | 0.0192 | H-15→LUMO (-13%), H-8→L+1 (19%), H-5→L+3 (-11%), H-1→L+7 (-17%) |
| 364.3 | 0.0824 | H-14→LUMO (-11%), H-9→L+1 (32%), H-8→L+1 (-31%) |
| 360.9 | 0.0051 | H-6→L+3 (85%) |
| 360.7 | 0.0245 | H-14→LUMO (44%), H-14→L+2 (-12%) |
| 358.4 | 0.0001 | H-8→L+2 (16%), H-2→L+5 (56%) |
| 358.3 | 0.0717 | H-13→LUMO (36%), H-9→L+1 (-33%) |
| 357.9 | 0.0028 | H-8→LUMO (12%), H-8→L+2 (50%), H-2→L+5 (-12%) |
| 356.6 | 0.033 | HOMO→L+8 (65%) |
| 353.3 | 0.0041 | H-10→L+1 (19%), H-9→L+2 (34%), HOMO→L+9 (-26%) |
| 352.4 | 0.0041 | H-10→L+1 (19%), H-1→L+8 (14%), HOMO→L+9 (47%) |
| 351.3 | 0.0053 | H-10→L+1 (41%), H-9→L+2 (-27%) |
| 351.2 | 0.0185 | H-7→L+3 (81%) |
| 346.6 | 0.0013 | H-12→L+1 (-18%), H-11→L+1 (25%), H-10→LUMO (10%), H-10→L+2 (35%) |
| 345.9 | 0 | H-3→L+4 (75%) |
| 345.7 | 0.0004 | H-11→L+1 (54%), H-10→L+2 (-18%) |
| 343.7 | 0 | H-13→L+1 (45%), H-11→L+2 (-20%) |
| 343.2 | 0.0064 | H-4→L+4 (93%) |
| 342.0 | 0.0032 | H-12→L+1 (73%), H-10→L+2 (15%) |
| 339.6 | 0.003 | H-8→L+3 (13%), H-1→L+8 (40%) |
| 338.6 | 0.0163 | H-9→L+3 (-20%), H-1→L+9 (29%) |
| 338.0 | 0.0022 | H-13→L+1 (20%), H-8→L+3 (36%) |
| 335.9 | 0.0031 | H-14→L+1 (31%), H-8→L+3 (20%) |
| 335.8 | 0.119 | H-26→L+1 (-12%), H-23→LUMO (24%), H-22→L+1 (-14%) |
| 334.9 | 0.0186 | H-12→LUMO (15%), H-12→L+2 (51%), H-1→L+9 (13%) |
| 334.3 | 0.0001 | H-23→L+1 (18%), H-22→LUMO (-11%), H-14→L+1 (28%) |
| 334.1 | 0.0003 | H-13→L+2 (-12%), H-10→L+3 (60%) |
| 332.7 | 0.0063 | H-9→L+3 (28%), H-1→L+9 (28%), HOMO→L+11 (-17%) |
| 332.4 | 0.0002 | H-14→L+1 (22%), H-11→L+2 (23%), H-5→L+4 (-12%) |
| 332.2 | 0.0549 | H-13→L+2 (50%), H-10→L+3 (13%) |
| 331.3 | 0.1277 | H-21→LUMO (40%), H-20→L+1 (-39%) |
| 331.0 | 0.0001 | H-21→L+1 (-32%), H-20→LUMO (33%) |
| 330.1 | 0.0001 | H-9→L+3 (19%), HOMO→L+11 (56%) |
| 329.9 | 0.0658 | H-15→L+3 (91%) |
| 329.3 | 0.0005 | H-5→L+4 (63%) |
| 326.9 | 0.0824 | H-14→L+2 (-23%), H-3→L+5 (-23%), HOMO→L+10 (27%) |
| 326.7 | 0.0556 | H-3→L+5 (22%), HOMO→L+10 (46%), HOMO→L+14 (-11%) |
| 326.5 | 0.0214 | H-14→LUMO (10%), H-14→L+2 (39%), H-3→L+5 (-28%) |
| 326.1 | 0 | H-15→L+1 (94%) |
| 324.1 | 0 | H-4→L+5 (95%) |
| 323.7 | 0.0394 | H-10→L+3 (13%), HOMO→L+12 (76%) |
| 322.6 | 0.0137 | H-3→L+5 (-13%), H-2→L+6 (35%) |
| 320.6 | 0.0024 | H-15→LUMO (32%), H-15→L+2 (49%) |
| 320.3 | 0.0011 | H-12→L+3 (29%), H-1→L+11 (28%) |
| 318.4 | 0.0009 | H-30→LUMO (17%), H-29→L+1 (-10%), H-22→LUMO (10%) |
| 317.7 | 0.054 | H-11→L+3 (80%) |
| 317.3 | 0.0071 | H-6→L+4 (75%) |
| 317.1 | 0.0002 | H-30→LUMO (24%), H-1→L+11 (-13%) |
| 316.2 | 0.0146 | H-14→L+3 (40%), H-13→L+3 (-21%), H-1→L+12 (29%) |
| 315.8 | 0.0259 | H-6→L+4 (12%), H-1→L+10 (22%) |
| 315.2 | 0.0004 | H-12→L+3 (44%), H-1→L+11 (-31%) |

Figure S16. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for AQ-[S]-[B-Zn]-[S]-AQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S8.Atomic contributions for the frontier MO for AQ-[S]-[B-Zn]-[S]-AQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2*thiophene-benzo-porphyrins | ~1.00 | 0.96 | 0.88 | 0.96 | ~1.00 | 0.42 | 0.10 | 0.63 | ~1.00 | 0.62 |
| 2*anthranquinone | ~0.0 | 0.04 | 0.12 | 0.04 | ~0.0 | 0.58 | 0.90 | 0.37 | ~0.0 | 0.38 |

NQ-[Zn]-NQ

Figure S17.Structure of NQ-[Zn]-NQ.

Figure S18.Image of the optimized structure ofNQ-[Zn]-NQ.

H-4 (-0.22199)

H-3 (-0.21712)

H-2 (-0.20605)

H-1 (-0.19991)

HOMO (-0.18054)

LUMO (-0.11329)

L+1 (-0.11213)

L+2 (-0.09887)

L+3 (-0.08713)

L+4  (-0.05050)

Figure S19.Representations of the frontier MOs ofNQ-[Zn]-NQ.The MO energies are in Hartree.

Table S9.Computed positions of the electronic transitions, oscillator strength (f), andmajor contributions of the NQ-[Zn]-NQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 793.5 | 0.7098 | HOMO→LUMO (97%) |
| 768.0 | 0 | HOMO→L+1 (98%) |
| 638.1 | 0.8064 | HOMO→L+2 (90%) |
| 610.5 | 0.0053 | H-1→LUMO (32%), H-1→L+2 (18%), HOMO→L+3 (50%) |
| 571.5 | 0 | H-1→L+1 (99%) |
| 570.8 | 0 | H-3→L+1 (-11%), H-2→LUMO (83%) |
| 565.9 | 0.033 | H-1→LUMO (67%), H-1→L+2 (-15%), HOMO→L+3 (-17%) |
| 561.3 | 0.0977 | H-3→LUMO (-14%), H-2→L+1 (78%) |
| 484.7 | 0.1518 | H-3→LUMO (71%), H-2→L+1 (17%) |
| 478.6 | 0.0001 | H-3→L+1 (51%), H-2→L+2 (36%) |
| 471.7 | 0 | H-3→L+1 (-29%), H-2→L+2 (63%) |
| 456.0 | 0.826 | H-1→L+2 (55%), HOMO→L+3 (-27%) |
| 453.1 | 0.0041 | H-4→LUMO (93%) |
| 452.6 | 1.1733 | H-3→L+2 (31%), H-1→L+3 (46%) |
| 444.5 | 0.1196 | H-5→LUMO (73%) |
| 443.5 | 0.0044 | H-14→LUMO (11%), H-13→LUMO (-30%), H-13→L+1 (41%) |
| 443.3 | 0.004 | H-4→L+1 (80%) |
| 443.2 | 0.0038 | H-14→LUMO (27%), H-14→L+1 (32%), H-4→L+1 (-18%) |
| 436.5 | 0 | H-5→L+1 (91%) |
| 430.8 | 0 | H-2→L+3 (96%) |
| 415.9 | 0.1747 | H-5→L+2 (34%), H-3→L+2 (39%), H-1→L+3 (-13%) |
| 415.8 | 0.0011 | H-4→L+2 (92%) |
| 408.0 | 0.0005 | H-8→LUMO (11%), H-6→LUMO (36%) |
| 407.4 | 0.0022 | H-27→L+1 (-10%), H-8→L+1 (-10%), H-7→LUMO (29%) |
| 404.8 | 0.0001 | H-8→LUMO (-11%), H-6→LUMO (55%) |
| 398.9 | 0.103 | H-7→LUMO (10%), H-5→L+2 (36%) |
| 397.9 | 0.034 | H-7→LUMO (-17%), H-6→L+1 (30%) |
| 397.2 | 0.0022 | H-7→LUMO (22%), H-6→L+1 (63%) |
| 393.3 | 0.0445 | H-9→LUMO (25%), H-9→L+2 (41%), H-3→L+3 (18%) |
| 392.2 | 0 | H-7→L+1 (-28%), H-4→L+3 (-18%), HOMO→L+4 (42%) |
| 391.3 | 0.0005 | H-7→L+1 (49%), H-4→L+3 (-26%), HOMO→L+4 (13%) |
| 389.3 | 0.4088 | H-5→L+2 (13%), H-3→L+3 (35%) |
| 388.5 | 0.0006 | H-4→L+3 (52%), HOMO→L+4 (35%) |
| 384.7 | 0.0002 | H-27→LUMO (-10%), H-8→LUMO (53%) |
| 380.3 | 0.0157 | H-27→L+1 (-10%), H-8→L+1 (63%) |
| 376.4 | 0.0009 | H-6→L+2 (85%) |
| 373.5 | 0.1025 | H-10→LUMO (39%), H-10→L+2 (21%), H-5→L+3 (25%) |
| 371.4 | 0.0859 | H-7→L+2 (48%), H-5→L+3 (14%) |
| 370.7 | 0.0158 | H-11→LUMO (51%), H-11→L+2 (23%) |
| 367.0 | 0.2066 | H-10→LUMO (25%), H-7→L+2 (31%), H-5→L+3 (-20%) |
| 364.0 | 0.0001 | H-9→L+1 (67%), H-8→L+2 (15%) |
| 362.7 | 0.0003 | H-12→LUMO (14%), H-9→L+1 (-32%), H-8→L+2 (35%) |
| 358.7 | 0.0248 | H-9→L+3 (90%) |
| 358.7 | 0.0042 | H-9→LUMO (59%), H-9→L+2 (-37%) |
| 357.6 | 0.0001 | H-10→L+1 (88%) |
| 355.7 | 0.0078 | H-11→L+1 (88%) |
| 354.6 | 0.0012 | H-6→L+3 (94%) |
| 351.3 | 0.0177 | H-12→L+1 (-27%), HOMO→L+5 (33%) |
| 350.0 | 0.0002 | H-12→LUMO (42%), H-8→L+2 (-29%) |
| 349.1 | 0.052 | H-12→L+1 (-13%), H-10→L+2 (-12%), H-7→L+3 (27%), HOMO→L+5 (-18%) |
| 347.5 | 0.0059 | H-12→L+1 (10%), H-10→LUMO (12%), H-10→L+2 (-23%), HOMO→L+5 (32%) |
| 347.3 | 0.0001 | H-11→LUMO (-35%), H-11→L+2 (49%) |
| 346.5 | 0 | HOMO→L+6 (80%) |
| 345.1 | 0.0461 | H-10→L+2 (26%), H-7→L+3 (44%) |
| 343.6 | 0.0297 | H-21→LUMO (17%), H-18→LUMO (-26%), H-17→L+1 (28%) |
| 343.4 | 0.0008 | H-21→L+1 (11%), H-18→L+1 (-25%), H-17→LUMO (34%) |
| 341.7 | 0.0015 | H-21→L+1 (-21%), H-19→LUMO (24%), H-18→L+1 (-11%) |
| 341.4 | 0.1484 | H-21→LUMO (20%), H-19→L+1 (-17%), H-18→LUMO (15%) |
| 335.7 | 0.0001 | H-1→L+4 (93%) |
| 335.6 | 0.0562 | H-16→L+2 (-10%), H-15→LUMO (35%), H-10→L+3 (23%) |
| 334.2 | 0.0001 | H-15→L+1 (15%), H-12→L+2 (14%), H-8→L+3 (15%) |
| 334.0 | 0.0001 | H-8→L+3 (62%) |
| 332.4 | 0.0379 | H-16→LUMO (17%), H-15→LUMO (15%), H-12→L+1 (33%) |
| 328.0 | 0.0002 | H-15→L+1 (13%), H-12→LUMO (10%), H-12→L+2 (-27%), H-11→L+3 (33%) |
| 327.9 | 0.0323 | H-16→LUMO (24%), H-15→LUMO (-10%), H-10→L+3 (52%) |
| 324.3 | 0.0661 | HOMO→L+7 (71%) |
| 323.7 | 0 | H-16→L+1 (-32%), H-15→L+1 (34%), H-11→L+3 (-23%) |
| 321.5 | 0 | H-16→L+1 (-19%), H-12→L+2 (32%), H-11→L+3 (32%) |
| 319.8 | 0.0014 | H-13→LUMO (43%), H-13→L+1 (38%) |
| 319.5 | 0.0021 | H-14→LUMO (-40%), H-14→L+1 (41%) |
| 318.2 | 0.2709 | H-2→L+4 (76%) |
| 315.4 | 0.0905 | H-24→LUMO (-16%), H-23→L+1 (18%), H-16→L+2 (12%), H-15→LUMO (16%) |
| 314.8 | 0.0002 | H-23→LUMO (-12%), H-16→L+1 (-11%), HOMO→L+8 (43%) |
| 314.5 | 0.007 | H-25→LUMO (38%), H-25→L+2 (23%) |
| 314.1 | 0.0017 | H-26→LUMO (33%), H-26→L+2 (19%), HOMO→L+8 (17%) |
| 314.0 | 0.0003 | H-26→LUMO (-16%), H-26→L+2 (-10%), H-23→LUMO (12%), HOMO→L+8 (22%) |
| 312.8 | 0.0014 | H-16→LUMO (-16%), H-16→L+2 (23%), H-15→L+2 (-21%) |
| 310.7 | 0.0001 | H-20→LUMO (60%), H-19→LUMO (17%) |
| 309.4 | 0.0079 | H-18→LUMO (31%), H-17→L+1 (30%) |
| 309.0 | 0.0006 | H-22→LUMO (47%), H-18→L+1 (17%), H-17→LUMO (14%) |
| 308.9 | 0.0007 | H-22→LUMO (32%), H-18→L+1 (-26%), H-17→LUMO (-18%) |
| 306.7 | 0 | H-21→L+1 (-11%), H-20→L+1 (65%), H-19→L+1 (17%) |
| 306.3 | 0.0001 | H-12→L+3 (79%), H-8→L+3 (-10%) |
| 305.1 | 0.0006 | H-22→L+1 (85%) |
| 305.0 | 0.0044 | H-16→L+2 (17%), H-15→L+2 (19%), H-13→L+2 (18%) |
| 302.6 | 0.0001 | H-21→L+1 (17%), H-19→LUMO (33%), H-19→L+1 (20%) |
| 302.3 | 0.0005 | H-21→LUMO (33%), H-21→L+1 (-10%), H-20→L+1 (-13%), H-19→L+1 (19%) |
| 302.0 | 0 | H-21→L+1 (14%), H-14→L+2 (29%) |
| 301.9 | 0.0026 | H-1→L+5 (82%) |
| 300.7 | 0.0011 | H-26→L+1 (34%), H-25→L+2 (-26%), H-13→L+2 (13%) |
| 300.6 | 0.0008 | H-26→L+2 (-36%), H-25→L+1 (50%) |
| 300.3 | 0.0011 | H-15→L+2 (-11%), H-13→L+2 (24%), H-3→L+4 (12%), H-2→L+5 (-18%) |
| 300.2 | 0.0011 | H-14→L+2 (14%), H-3→L+4 (-18%), H-2→L+5 (23%) |
| 298.4 | 0.1178 | H-16→L+3 (46%), H-15→L+3 (-35%), H-1→L+5 (-12%) |
| 298.4 | 0.0024 | H-17→L+2 (-24%), H-14→L+2 (31%), HOMO→L+10 (23%) |
| 298.1 | 0.0012 | H-1→L+6 (93%) |
| 297.7 | 0.0506 | H-18→L+2 (27%), H-13→L+2 (15%), HOMO→L+9 (29%) |
| 293.9 | 0.1712 | H-3→L+5 (-10%), H-2→L+6 (70%) |
| 293.1 | 0.0002 | H-3→L+4 (49%), H-2→L+5 (23%) |

Figure S20.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[Zn]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S10.Atomic contributions for the frontier MO for NQ-[Zn]-NQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ethyne-porphyrins | 1.00 | 0.39 | 0.19 | ~1.00 | 0.72 | 0.07 | 0.01 | 0.80 | ~1.00 | 0.52 |
| 2*naphtoquinone | 0.00 | 0.61 | 0.81 | ~0.00 | 0.28 | 0.93 | 0.99 | 0.20 | ~0.00 | 0.48 |

NQ-[S]-[Zn]-[S]-NQ

Figure S21.Structure of NQ-[S]-[Zn]-[S]-NQ.

Figure S22.Image of the optimized structure ofNQ-[S]-[Zn]-[S]-NQ.

H-4 (-0.21540)

H-3 (-0.20079)

H-2 (-0.19737)

H-1 (-0.19110)

HOMO (-0.17450)

LUMO (-0.10696)

L+1 (-0.10610)

L+2 (-0.10103)

L+3 (-0.08409)

L+4  (-0.06708)

Figure S23. Representations of the frontier MOs ofNQ-[S]-[Zn]-[S]-NQ.The MO energies are in Hartree.

Table S11.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the NQ-[S]-[Zn]-[S]-NQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 778.1 | 1.7224 | HOMO→LUMO (86%) |
| 746.6 | 0.0671 | HOMO→L+1 (93%) |
| 702.6 | 0.8658 | HOMO→L+2 (89%) |
| 621.6 | 0.0911 | H-3→L+1 (13%), H-1→LUMO (77%) |
| 620.6 | 0.0049 | H-2→LUMO (-10%), H-2→L+2 (26%), HOMO→L+3 (62%) |
| 612.7 | 0.0927 | H-3→LUMO (15%), H-1→L+1 (73%) |
| 562.6 | 0.0225 | H-1→L+2 (93%) |
| 534.0 | 0.0437 | H-3→LUMO (26%), H-2→LUMO (45%), H-2→L+1 (10%) |
| 533.2 | 0.0574 | H-3→LUMO (39%), H-2→LUMO (-14%), H-2→L+1 (-30%) |
| 530.9 | 0.023 | H-2→LUMO (-28%), H-2→L+1 (60%) |
| 524.2 | 0.0088 | H-3→L+1 (73%), H-1→LUMO (-16%) |
| 508.3 | 0.2583 | H-3→L+2 (73%), H-2→L+3 (-12%) |
| 487.4 | 0.595 | H-2→L+2 (56%), HOMO→L+3 (-31%) |
| 472.5 | 0.0722 | H-1→L+3 (-41%), HOMO→L+4 (55%) |
| 472.4 | 0.0585 | H-1→L+3 (55%), HOMO→L+4 (41%) |
| 461.8 | 0.0008 | H-4→LUMO (52%), H-4→L+2 (-43%) |
| 455.5 | 0.0803 | H-5→LUMO (46%), H-5→L+2 (-29%) |
| 451.6 | 1.6608 | H-3→L+2 (12%), H-2→L+3 (42%), HOMO→L+5 (-24%) |
| 450.4 | 0.0478 | H-6→LUMO (51%), H-5→L+1 (11%) |
| 447.1 | 0.0799 | H-6→L+1 (26%), H-5→L+2 (18%), H-4→L+1 (-10%) |
| 445.4 | 0.0018 | H-15→LUMO (36%), H-15→L+1 (37%) |
| 444.9 | 0.0097 | H-14→LUMO (-26%), H-14→L+1 (40%) |
| 437.6 | 0.0023 | H-6→L+1 (15%), H-4→L+1 (66%) |
| 434.1 | 0.002 | H-4→LUMO (39%), H-4→L+2 (43%) |
| 431.0 | 0.0008 | H-5→L+1 (75%) |
| 426.8 | 0.0083 | H-6→L+1 (-10%), H-5→LUMO (42%), H-5→L+2 (37%) |
| 420.2 | 0.0632 | H-6→L+2 (71%) |
| 419.5 | 0.4276 | H-6→L+2 (-10%), H-3→L+3 (65%) |
| 413.2 | 0.0043 | H-7→LUMO (34%), H-7→L+2 (-33%), HOMO→L+5 (17%) |
| 411.1 | 0.0018 | H-8→LUMO (-39%), H-8→L+2 (45%) |
| 406.4 | 0.0161 | H-9→L+2 (12%), H-7→LUMO (-15%), HOMO→L+5 (30%) |
| 404.1 | 0.0089 | H-10→LUMO (-20%), H-10→L+2 (64%) |
| 402.4 | 0.0074 | H-29→LUMO (-12%), H-7→L+1 (12%) |
| 401.8 | 0.0031 | H-4→L+3 (85%) |
| 401.7 | 0.004 | H-29→L+1 (15%) |
| 397.5 | 0.3545 | H-5→L+3 (25%), H-1→L+4 (54%) |
| 395.1 | 0.0145 | H-7→L+1 (54%) |
| 393.1 | 0.0213 | H-5→L+3 (38%), H-1→L+4 (-10%) |
| 390.8 | 0.0113 | H-8→L+1 (38%), H-7→L+1 (-11%), H-7→L+2 (14%) |
| 390.2 | 0.0046 | H-8→L+1 (51%), H-7→LUMO (-15%), H-7→L+2 (-19%) |
| 387.6 | 0.0052 | H-8→LUMO (43%), H-8→L+2 (36%) |
| 386.5 | 0.0001 | H-2→L+4 (91%) |
| 376.9 | 0.0111 | H-9→LUMO (19%), H-9→L+1 (52%) |
| 375.8 | 0.0081 | H-9→LUMO (38%), H-9→L+1 (-21%) |
| 375.6 | 0.0005 | H-13→LUMO (-21%), H-13→L+2 (50%), H-6→L+3 (-16%) |
| 373.6 | 0.0116 | H-11→LUMO (-27%), H-11→L+2 (58%) |
| 369.7 | 0.1004 | H-12→LUMO (-14%), H-12→L+2 (30%), H-3→L+4 (39%) |
| 366.7 | 0.0017 | H-13→L+2 (10%), H-8→L+3 (14%), H-6→L+3 (60%) |
| 366.2 | 0.0762 | H-12→LUMO (14%), H-12→L+2 (-23%), H-3→L+4 (34%), H-1→L+5 (12%) |
| 365.6 | 0.0189 | H-9→L+2 (37%), H-7→L+3 (31%) |
| 362.7 | 0.0021 | H-8→L+3 (71%), H-6→L+3 (-11%) |
| 361.5 | 0.0015 | H-10→L+3 (94%) |
| 358.7 | 0.0571 | H-9→L+2 (-19%), H-7→L+3 (44%) |
| 358.1 | 0.0934 | H-3→L+4 (-12%), H-1→L+5 (62%), HOMO→L+6 (14%) |
| 354.4 | 0.0134 | H-1→L+5 (-12%), HOMO→L+6 (58%), HOMO→L+8 (-15%) |
| 351.0 | 0.0011 | H-10→LUMO (17%), H-10→L+1 (75%) |
| 349.6 | 0.0005 | H-10→LUMO (52%), H-10→L+1 (-21%), H-10→L+2 (18%) |
| 349.2 | 0.1517 | H-2→L+5 (91%) |
| 347.0 | 0.0065 | H-12→L+1 (34%) |
| 345.7 | 0.0056 | H-12→LUMO (20%), H-12→L+2 (12%) |
| 343.7 | 0.0005 | H-13→L+1 (-10%), H-11→LUMO (13%), H-11→L+1 (48%) |
| 342.4 | 0.002 | H-13→L+1 (30%), H-11→LUMO (-14%), H-11→L+1 (17%), HOMO→L+7 (-16%) |
| 342.2 | 0.0078 | H-12→L+1 (14%), HOMO→L+7 (33%) |
| 341.5 | 0.0176 | H-23→LUMO (25%), H-22→L+1 (17%), HOMO→L+8 (11%) |
| 340.9 | 0.023 | H-23→L+1 (-16%), H-21→L+1 (-11%), H-18→LUMO (22%), HOMO→L+7 (-12%) |
| 340.4 | 0.0528 | H-23→L+1 (11%), H-22→LUMO (14%), H-21→LUMO (-14%), H-18→L+1 (11%) |
| 340.1 | 0.0144 | H-21→LUMO (-10%), H-21→L+1 (12%), H-18→L+1 (12%), HOMO→L+8 (10%) |
| 340.0 | 0.0086 | H-13→LUMO (18%), H-13→L+1 (28%), H-11→LUMO (23%) |
| 339.5 | 0.0187 | H-23→LUMO (-10%), H-22→L+1 (-12%), H-12→LUMO (-10%), HOMO→L+8 (30%) |
| 338.9 | 0.0004 | H-13→LUMO (37%), H-13→L+1 (-20%), H-13→L+2 (16%), H-11→L+1 (11%) |
| 338.1 | 0.0179 | H-17→LUMO (-16%), H-17→L+2 (36%), H-11→L+3 (16%) |
| 334.5 | 0.0282 | H-12→L+1 (10%) |
| 333.9 | 0.0122 | H-16→LUMO (10%) |
| 332.3 | 0.2312 | H-3→L+5 (68%) |
| 330.2 | 0.0174 | H-4→L+4 (87%) |
| 327.2 | 0.0543 | H-11→L+3 (34%), H-9→L+3 (-12%), H-5→L+4 (31%) |
| 326.7 | 0.0334 | H-11→L+3 (-14%), H-5→L+4 (64%) |
| 325.8 | 0.187 | H-11→L+3 (19%), H-9→L+3 (61%) |
| 325.1 | 0.002 | H-12→L+3 (81%) |
| 324.8 | 0.0019 | H-13→L+3 (92%) |
| 319.6 | 0.0329 | H-6→L+4 (79%) |
| 319.0 | 0.0054 | H-16→LUMO (-12%), H-16→L+2 (18%), H-15→LUMO (-13%), H-15→L+1 (12%), H-14→LUMO (-13%) |
| 318.5 | 0.0003 | H-15→LUMO (27%), H-15→L+1 (-14%), H-14→LUMO (-26%), H-14→L+1 (-19%) |
| 317.9 | 0.0046 | H-16→LUMO (-15%), H-16→L+2 (17%), H-15→L+1 (-11%), H-14→LUMO (20%) |
| 315.0 | 0.0775 | H-1→L+6 (50%) |
| 314.0 | 0.0007 | H-19→LUMO (54%), H-19→L+2 (-25%) |
| 313.3 | 0.0303 | H-25→LUMO (-13%), H-24→LUMO (38%) |
| 312.9 | 0.0082 | H-25→LUMO (40%), H-25→L+1 (-12%), H-24→LUMO (11%) |
| 312.7 | 0.0005 | H-20→LUMO (38%), H-20→L+2 (-28%) |
| 312.4 | 0.0039 | H-17→L+1 (36%), H-15→L+2 (-11%) |
| 312.0 | 0.0059 | H-17→L+1 (30%), H-15→L+2 (39%) |
| 311.9 | 0.0015 | H-17→L+1 (10%), H-15→L+2 (-18%), H-14→L+1 (11%), H-14→L+2 (47%) |
| 311.4 | 0.0422 | H-17→L+1 (15%), H-16→L+1 (24%), H-1→L+6 (11%) |
| 311.2 | 0.009 | H-16→L+2 (20%), H-14→L+2 (-21%), H-1→L+7 (21%) |
| 310.2 | 0.0239 | H-17→LUMO (41%), H-17→L+2 (25%) |
| 308.7 | 0.0035 | HOMO→L+9 (52%) |
| 308.3 | 0.0103 | HOMO→L+10 (38%) |
| 308.0 | 0.0001 | H-36→L+2 (10%), H-32→L+2 (-11%), H-31→LUMO (-10%), H-31→L+2 (13%), HOMO→L+9 (-11%) |
| 307.7 | 0.0044 | H-31→LUMO (-13%), H-31→L+2 (18%) |

Figure S24.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[S]-[Zn]-[S]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S12.Atomic contributions for the frontier MO for NQ-[S]-[Zn]-[S]-NQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2*thiopene-porphyrins | 0.97 | 0.40 | ~1.00 | 0.47 | 0.87 | 0.16 | 0.02 | 0.81 | ~1.00 | 0.81 |
| 2*naphtoquinone | 0.03 | 0.60 | ~0.0 | 0.53 | 0.13 | 0.84 | 0.98 | 0.19 | ~0.0 | 0.19 |

NQ-[B-Zn]-NQ

Figure S25.Structure of NQ-[B-Zn]-NQ.

Figure S26.Image of the optimized structure of NQ-[B-Zn]-NQ.

H-4   (-0.21413)

H-3  (-0.20874)

H-2  (-0.19662)

H-1  (-0.17524)

HOMO  (-0.17222)

LUMO  (-0.10608)

L+1  (-0.10519)

L+2  (-0.09055)

L+3 (-0.08010)

L+4  (-0.04596)

Figure S27. Representations of the frontier MOs of NQ-[B-Zn]-NQ.The MO energies are inHartree.

Table S13.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the NQ-[B-Zn]-NQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 786.9 | 0.0331 | HOMO→LUMO (97%) |
| 774.4 | 0.6035 | H-1→LUMO (90%) |
| 773.3 | 0.015 | HOMO→L+1 (97%) |
| 751.6 | 0.0004 | H-1→L+1 (96%) |
| 671.7 | 0.1108 | H-1→L+3 (24%), HOMO→L+2 (74%) |
| 655.1 | 0.0913 | H-1→L+2 (66%), HOMO→L+3 (-31%) |
| 583.9 | 0.0047 | H-3→L+1 (-10%), H-2→LUMO (83%) |
| 578.3 | 0.3697 | H-3→LUMO (-13%), H-2→L+1 (74%) |
| 526.7 | 2.0594 | H-1→L+2 (28%), HOMO→L+3 (55%) |
| 510.8 | 1.0643 | H-1→L+3 (74%), HOMO→L+2 (-25%) |
| 488.2 | 0.1133 | H-3→LUMO (69%), H-2→L+1 (11%) |
| 487.4 | 0.0076 | H-3→L+1 (42%), H-2→L+2 (-38%) |
| 481.7 | 0.0012 | H-3→L+1 (32%), H-2→L+2 (58%) |
| 456.1 | 0.0001 | H-4→LUMO (92%) |
| 450.3 | 0.0022 | H-5→LUMO (-45%), H-4→L+1 (46%) |
| 446.0 | 0.001 | H-5→LUMO (33%), H-4→L+1 (49%) |
| 445.5 | 0.0005 | H-17→LUMO (32%), H-16→LUMO (-13%), H-16→L+1 (-32%) |
| 445.2 | 0.0008 | H-17→LUMO (-13%), H-17→L+1 (32%), H-16→LUMO (-28%), H-16→L+1 (14%) |
| 442.7 | 0.0042 | H-2→L+3 (89%) |
| 440.6 | 0.0003 | H-5→L+1 (82%) |
| 426.1 | 0.0481 | H-3→L+2 (83%) |
| 420.2 | 0.0006 | H-6→LUMO (73%) |
| 417.2 | 0.0002 | H-4→L+2 (91%) |
| 416.8 | 0.0025 | H-8→L+1 (-14%), H-7→LUMO (14%), H-6→L+1 (41%) |
| 411.2 | 0 | H-8→LUMO (35%), H-7→L+1 (-13%), H-6→LUMO (15%) |
| 408.8 | 0.0001 | H-7→LUMO (-22%), H-6→L+1 (53%) |
| 406.1 | 0.0462 | HOMO→L+4 (88%) |
| 404.8 | 0.0407 | H-5→L+2 (77%) |
| 400.4 | 0.0012 | H-31→L+1 (-10%), H-7→LUMO (52%) |
| 397.7 | 0.0002 | H-1→L+4 (79%) |
| 396.2 | 0.0013 | H-7→L+1 (69%), H-1→L+4 (11%) |
| 396.0 | 0.1718 | H-5→L+3 (-14%), H-3→L+3 (81%) |
| 393.8 | 0.001 | H-31→LUMO (11%), H-8→LUMO (43%) |
| 391.0 | 0.0055 | H-31→L+1 (11%), H-8→L+1 (57%) |
| 389.8 | 0.0005 | H-4→L+3 (97%) |
| 386.4 | 0.0077 | H-9→LUMO (26%), H-6→L+2 (54%) |
| 384.5 | 0.0012 | H-9→LUMO (53%), H-6→L+2 (-35%) |
| 380.2 | 0.0038 | H-10→LUMO (42%), H-9→L+1 (-37%) |
| 377.9 | 0.0539 | H-9→L+1 (15%), H-5→L+3 (68%), H-3→L+3 (10%) |
| 373.2 | 0.0148 | H-7→L+2 (75%) |
| 372.9 | 0.002 | H-11→LUMO (49%), H-11→L+2 (-10%), H-8→L+2 (14%) |
| 372.6 | 0.0027 | H-10→LUMO (35%), H-9→L+1 (35%) |
| 368.2 | 0.0001 | H-10→L+1 (80%) |
| 366.8 | 0.0003 | H-12→LUMO (-32%), H-11→L+1 (46%) |
| 365.2 | 0.0003 | H-11→LUMO (-12%), H-9→L+2 (-18%), H-8→L+2 (38%), H-6→L+3 (-10%) |
| 361.8 | 0.0918 | H-15→LUMO (-36%), H-15→L+2 (53%) |
| 361.4 | 0.0052 | H-8→L+2 (11%), H-6→L+3 (69%) |
| 360.8 | 0.0026 | H-13→LUMO (-26%), H-9→L+2 (29%), H-8→L+2 (16%) |
| 359.2 | 0.0088 | H-12→LUMO (50%), H-11→L+1 (30%) |
| 357.9 | 0.0575 | HOMO→L+5 (67%), HOMO→L+7 (-20%) |
| 357.3 | 0.0041 | H-13→LUMO (50%), H-10→L+1 (10%), H-9→L+2 (25%) |
| 356.7 | 0.0006 | H-12→L+1 (70%) |
| 354.9 | 0.0064 | H-13→L+1 (44%), H-10→L+2 (-35%) |
| 354.0 | 0.2165 | H-14→LUMO (24%), H-1→L+5 (39%) |
| 352.5 | 0.0002 | HOMO→L+8 (70%) |
| 352.0 | 0.0065 | H-14→LUMO (13%), H-13→L+1 (35%), H-10→L+2 (22%), H-7→L+3 (-11%) |
| 351.7 | 0.0257 | H-14→LUMO (-21%), H-7→L+3 (-25%), H-1→L+5 (29%) |
| 350.8 | 0.0014 | H-14→LUMO (-12%), H-10→L+2 (15%), H-7→L+3 (50%) |
| 349.4 | 0.0019 | H-1→L+8 (24%), HOMO→L+6 (50%), HOMO→L+9 (11%) |
| 347.9 | 0.0001 | H-14→L+1 (32%), H-11→L+2 (-24%), H-1→L+6 (-12%) |
| 346.3 | 0.0002 | H-14→L+1 (42%), H-1→L+6 (21%) |
| 345.3 | 0.0011 | H-8→L+3 (-27%), H-1→L+8 (-16%), HOMO→L+6 (27%) |
| 343.9 | 0.0495 | H-20→L+1 (-12%), H-19→LUMO (34%), H-18→L+1 (-22%) |
| 343.6 | 0.0031 | H-14→L+1 (10%), H-11→L+2 (20%) |
| 342.4 | 0.0012 | H-15→L+1 (20%), H-1→L+6 (32%) |
| 341.7 | 0.0026 | H-20→LUMO (-10%), H-15→L+1 (53%) |
| 341.2 | 0.0603 | H-25→LUMO (17%), H-24→LUMO (-14%), H-24→L+1 (25%) |
| 340.8 | 0.0077 | HOMO→L+5 (23%), HOMO→L+7 (70%) |
| 340.6 | 0.0001 | H-25→L+1 (14%), H-24→LUMO (23%), H-24→L+1 (-15%), H-15→L+1 (15%) |
| 339.8 | 0.1458 | H-21→LUMO (20%), H-20→L+1 (11%), H-1→L+7 (11%) |
| 339.0 | 0.0034 | H-13→L+2 (20%), H-8→L+3 (39%), H-1→L+8 (-17%) |
| 338.6 | 0.0026 | H-14→L+2 (10%), H-12→L+2 (52%) |
| 337.9 | 0.0031 | H-13→L+2 (10%), H-1→L+6 (10%), HOMO→L+9 (11%) |
| 337.9 | 0.0017 | H-13→L+2 (37%), HOMO→L+9 (13%) |
| 336.9 | 0.0139 | H-15→LUMO (50%), H-15→L+2 (32%) |
| 336.3 | 0.028 | H-12→L+2 (-13%), H-10→L+3 (26%), H-1→L+7 (10%) |
| 335.2 | 0.0472 | H-13→L+2 (-12%), H-1→L+8 (-23%), HOMO→L+9 (42%), HOMO→L+10 (-11%) |
| 334.1 | 0.0102 | H-14→L+2 (-21%), H-1→L+7 (38%) |
| 333.5 | 0.0359 | H-15→L+3 (71%), H-9→L+3 (17%) |
| 333.1 | 0.0102 | H-15→L+3 (-23%), H-9→L+3 (51%) |
| 331.0 | 0.2514 | H-2→L+4 (70%) |
| 329.0 | 0.0001 | H-1→L+9 (73%) |
| 327.9 | 0.007 | H-14→L+2 (-32%), H-10→L+3 (34%), H-2→L+4 (11%) |
| 324.1 | 0.0429 | H-10→L+3 (15%), HOMO→L+11 (73%) |
| 322.5 | 0.0497 | H-11→L+3 (80%) |
| 321.0 | 0.0005 | H-26→LUMO (27%), H-22→LUMO (-13%), H-20→LUMO (-11%) |
| 319.6 | 0 | H-17→LUMO (34%), H-17→L+1 (17%), H-16→LUMO (18%), H-16→L+1 (28%) |
| 319.4 | 0 | H-17→LUMO (-16%), H-17→L+1 (30%), H-16→LUMO (30%), H-16→L+1 (-21%) |
| 318.2 | 0.0021 | H-14→L+3 (16%), H-1→L+11 (74%) |
| 317.4 | 0.0047 | H-27→LUMO (21%), H-26→L+1 (16%), H-18→L+1 (11%) |
| 316.6 | 0.0298 | H-14→L+3 (11%), H-12→L+3 (73%), HOMO→L+12 (-10%) |
| 315.5 | 0.0333 | HOMO→L+9 (15%), HOMO→L+10 (73%) |
| 314.4 | 0 | H-18→LUMO (14%), H-13→L+3 (51%) |
| 314.2 | 0.1218 | H-14→L+3 (16%), HOMO→L+12 (62%) |
| 313.1 | 0.0004 | H-19→L+1 (13%), H-18→LUMO (30%), H-13→L+3 (-22%) |
| 311.4 | 0.0142 | H-19→LUMO (21%), H-18→L+1 (42%) |
| 310.9 | 0.0222 | H-14→L+3 (50%), H-12→L+3 (-17%), H-1→L+11 (-18%) |
| 310.8 | 0.0394 | H-20→L+1 (12%) |
| 310.5 | 0.0011 | H-1→L+10 (60%) |

Figure S28.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[B-Zn]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S14.Atomic contributions for the frontier MO for NQ-[B-Zn]-NQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| benzo-porphyrins | ~1.00 | 0.43 | 0.29 | 0.74 | 0.99 | 0.06 | 0.01 | 0.85 | 0.99 | 0.61 |
| 2*naphtoquinone | ~0.0 | 0.57 | 0.71 | 0.26 | 0.01 | 0.94 | 0.99 | 0.15 | 0.01 | 0.39 |

NQ-[S]-[B-Zn]-[S]-NQ

Figure S29.Structure of NQ-[S]-[B-Zn]-[S]-NQ.

Figure S30.Image of the optimized structure of NQ-[S]-[B-Zn]-[S]-NQ.

H-4   (-0.21401)

H-3  (-0.19968)

H-2  (-0.18995)

H-1  (-0.17539)

HOMO  (-0.17348)

LUMO  (-0.10621)

L+1  (-0.10582)

L+2  (-0.09694)

L+3 (-0.08130)

L+4  (-0.06764)

Figure S31. Representations of the frontier MOs of NQ-[S]-[B-Zn]-[S]-NQ.The MO energies are in Hartree.

Table S15.Computed positions of the electronic transitions,oscillator strength (f), and major contributions of the NQ-[S]-[B-Zn]-[S]-NQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 754.8 | 1.0425 | H-1→LUMO (76%) |
| 747.3 | 0.1286 | HOMO→LUMO (83%) |
| 736.8 | 0.0017 | H-1→L+1 (19%), HOMO→L+1 (79%) |
| 733.7 | 0.003 | H-1→L+1 (72%), HOMO→L+1 (-21%) |
| 700.9 | 0.125 | H-1→L+3 (14%), HOMO→LUMO (10%), HOMO→L+2 (74%) |
| 688.3 | 0.4467 | H-1→LUMO (11%), H-1→L+2 (73%), HOMO→L+3 (-14%) |
| 621.7 | 0.0032 | H-3→L+1 (14%), H-2→LUMO (74%) |
| 617.7 | 0.3036 | H-3→LUMO (16%), H-2→L+1 (70%) |
| 560.8 | 2.2122 | H-3→L+2 (-12%), H-1→L+2 (14%), HOMO→L+3 (61%) |
| 548.8 | 0.0016 | H-2→L+2 (94%) |
| 531.1 | 0.1683 | H-3→LUMO (70%), H-2→L+1 (-16%) |
| 530.0 | 0.0054 | H-3→L+1 (71%), H-2→LUMO (-17%) |
| 527.2 | 0.7148 | H-1→L+3 (79%), HOMO→L+2 (-17%) |
| 488.8 | 0.009 | HOMO→L+4 (97%) |
| 478.1 | 0.3699 | H-3→L+2 (78%) |
| 475.4 | 0.0028 | H-1→L+4 (96%) |
| 466.6 | 0.006 | H-2→L+3 (93%) |
| 460.7 | 0.0002 | H-6→LUMO (-27%), H-4→LUMO (41%) |
| 459.3 | 0.0158 | H-6→L+1 (-30%), H-5→LUMO (16%), H-4→L+1 (30%) |
| 450.1 | 0.0013 | H-6→LUMO (33%), H-4→LUMO (24%), H-4→L+2 (-31%) |
| 445.5 | 0.0029 | H-18→LUMO (-34%), H-18→L+1 (48%) |
| 445.2 | 0.0017 | H-19→LUMO (46%), H-19→L+1 (35%) |
| 444.6 | 0.0185 | H-5→LUMO (40%), H-5→L+2 (-31%) |
| 440.6 | 0.0035 | H-6→L+1 (37%), H-4→L+1 (58%) |
| 437.6 | 0.095 | H-3→L+3 (12%), HOMO→L+5 (83%) |
| 436.9 | 0 | H-6→LUMO (16%), H-5→L+1 (69%), H-4→L+2 (13%) |
| 433.9 | 0.0005 | H-5→L+1 (-20%), H-4→LUMO (29%), H-4→L+2 (43%) |
| 429.5 | 0.0183 | H-5→LUMO (34%), H-5→L+2 (57%) |
| 421.6 | 0.0018 | H-6→L+2 (69%) |
| 418.4 | 0.1202 | H-1→L+5 (75%) |
| 416.0 | 0.4988 | H-3→L+3 (77%), HOMO→L+5 (-12%) |
| 412.6 | 0.0116 | H-7→LUMO (49%), H-6→L+1 (10%) |
| 411.8 | 0.0014 | H-8→LUMO (39%), H-8→L+2 (-11%), H-7→L+1 (12%), H-6→L+2 (16%) |
| 408.2 | 0.0018 | H-8→LUMO (-12%), H-8→L+2 (26%), H-7→L+1 (26%) |
| 405.1 | 0.3639 | H-7→L+2 (17%), H-2→L+4 (54%) |
| 403.5 | 0.3962 | H-7→L+2 (-13%), H-2→L+4 (33%) |
| 401.1 | 0.0039 | H-8→L+1 (64%) |
| 399.1 | 0.0005 | H-7→L+1 (33%) |
| 396.3 | 0.0017 | H-8→LUMO (37%), H-8→L+2 (43%) |
| 394.4 | 0.034 | H-7→LUMO (21%), H-7→L+2 (46%) |
| 393.4 | 0.0021 | H-6→L+3 (12%), H-4→L+3 (84%) |
| 388.0 | 0.0061 | H-5→L+3 (90%) |
| 385.2 | 0.001 | H-10→LUMO (-25%), H-10→L+2 (54%) |
| 385.0 | 0.0196 | H-9→LUMO (61%) |
| 383.5 | 0.0003 | H-9→L+1 (65%) |
| 376.6 | 0.0032 | H-12→LUMO (-25%), H-12→L+2 (56%) |
| 375.9 | 0.0019 | H-11→L+2 (22%), H-3→L+4 (45%), H-2→L+5 (-12%) |
| 374.8 | 0.0043 | H-11→LUMO (-14%), H-11→L+2 (26%), H-3→L+4 (-15%), H-2→L+5 (17%) |
| 373.2 | 0.002 | H-9→L+2 (59%) |
| 372.7 | 0.0026 | H-6→L+3 (62%) |
| 369.5 | 0.0013 | H-10→L+1 (90%) |
| 367.3 | 0.0035 | H-10→LUMO (55%), H-10→L+2 (25%) |
| 366.2 | 0.001 | H-3→L+4 (29%), H-2→L+5 (58%) |
| 365.5 | 0.0271 | HOMO→L+6 (47%), HOMO→L+8 (-23%) |
| 363.5 | 0.0192 | H-17→L+2 (61%) |
| 363.1 | 0.0029 | H-11→L+1 (63%) |
| 362.2 | 0.0005 | H-12→L+1 (-27%), H-11→LUMO (29%), H-11→L+2 (13%) |
| 360.5 | 0.0011 | H-8→L+3 (59%) |
| 359.1 | 0.0179 | H-7→L+3 (76%) |
| 358.9 | 0.0015 | H-12→L+1 (45%), H-11→LUMO (12%) |
| 358.3 | 0.0012 | H-1→L+6 (42%), H-1→L+8 (-15%), HOMO→L+9 (-26%) |
| 357.1 | 0.0011 | H-12→LUMO (64%), H-12→L+2 (24%) |
| 355.9 | 0.0322 | H-13→LUMO (-26%), H-13→L+2 (34%), H-12→L+1 (-10%) |
| 353.2 | 0.0325 | H-16→LUMO (-17%), H-16→L+2 (24%), H-15→LUMO (-11%), H-14→L+1 (22%) |
| 352.7 | 0.0019 | H-14→LUMO (38%), H-11→LUMO (-12%), H-11→L+2 (-13%), HOMO→L+9 (-12%) |
| 352.3 | 0.067 | H-16→LUMO (-10%), H-16→L+2 (31%), H-15→LUMO (17%), H-14→L+1 (-15%), H-11→L+1 (10%) |
| 349.4 | 0.0003 | H-14→L+2 (11%), H-1→L+6 (14%), HOMO→L+9 (45%) |
| 347.3 | 0.0001 | H-13→L+1 (90%) |
| 346.6 | 0.2062 | H-15→LUMO (-14%), H-15→L+2 (29%), H-14→L+1 (-10%), H-3→L+5 (22%) |
| 344.9 | 0.0003 | H-13→LUMO (51%), H-13→L+2 (29%) |
| 343.2 | 0.1897 | H-15→LUMO (10%), H-14→L+1 (12%), H-3→L+5 (40%) |
| 343.0 | 0.0419 | H-15→L+1 (-15%), H-14→L+2 (15%), H-1→L+6 (-13%) |
| 342.2 | 0.0286 | H-1→L+9 (44%), HOMO→L+6 (-29%) |
| 341.4 | 0.0494 | H-25→L+1 (-11%), H-20→L+1 (10%), H-1→L+7 (27%) |
| 341.0 | 0.0029 | H-25→LUMO (15%), H-24→L+1 (18%), H-21→L+1 (13%), H-20→LUMO (-13%) |
| 340.6 | 0.0017 | HOMO→L+7 (81%) |
| 340.4 | 0.0003 | H-16→L+1 (69%), H-15→L+1 (-11%) |
| 340.1 | 0.0021 | H-21→LUMO (-15%), H-20→LUMO (11%), H-20→L+1 (18%), H-1→L+7 (-12%) |
| 339.9 | 0.0014 | H-21→LUMO (-10%), H-21→L+1 (26%), H-20→LUMO (-10%) |
| 339.7 | 0.0545 | H-25→L+1 (14%), H-24→LUMO (14%), H-1→L+7 (21%) |
| 339.4 | 0.0022 | H-16→L+1 (19%), H-15→L+1 (28%), H-1→L+8 (-14%) |
| 338.7 | 0.0106 | H-16→LUMO (43%), H-16→L+2 (11%), H-15→LUMO (-11%), H-15→L+2 (-10%) |
| 338.1 | 0.0371 | H-1→L+9 (26%), HOMO→L+8 (55%) |
| 337.5 | 0.0145 | H-16→LUMO (21%), H-16→L+2 (10%), H-15→LUMO (19%), H-15→L+2 (23%), H-14→L+1 (10%) |
| 336.9 | 0.0013 | H-17→L+3 (42%), H-9→L+3 (-41%) |
| 336.1 | 0.001 | H-14→L+2 (33%), H-1→L+8 (31%) |
| 334.6 | 0.0097 | H-4→L+4 (69%) |
| 334.4 | 0.0019 | H-10→L+3 (70%) |
| 332.5 | 0.0048 | H-17→L+1 (62%) |
| 332.2 | 0.0247 | H-17→LUMO (-21%), H-17→L+1 (12%), H-12→L+3 (21%) |
| 331.9 | 0.0001 | H-11→L+3 (26%), HOMO→L+11 (41%), HOMO→L+13 (-13%) |
| 331.5 | 0.0276 | H-12→L+3 (36%) |
| 331.2 | 0.0001 | H-5→L+4 (91%) |
| 330.6 | 0.0009 | H-29→L+1 (-19%), H-28→LUMO (14%), H-17→L+1 (24%) |
| 330.2 | 0.0388 | H-29→LUMO (-11%), H-17→LUMO (47%) |
| 329.6 | 0.027 | H-6→L+4 (71%) |
| 328.6 | 0.0155 | H-11→L+3 (46%), HOMO→L+11 (-23%) |
| 327.4 | 0.0494 | H-17→L+3 (31%), H-9→L+3 (24%), HOMO→L+10 (12%) |
| 326.1 | 0.0012 | HOMO→L+10 (52%), HOMO→L+14 (23%) |
| 323.5 | 0.0168 | H-12→L+3 (14%), HOMO→L+12 (71%) |

Figure S32. Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[S]-[B-Zn]-[S]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S16.Atomic contributions for the frontier MO for NQ-[S]-[B-Zn]-[S]-NQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2*thiophene- benzo-porphyrins | 0.55 | 0.71 | 0.82 | 0.85 | 0.81 | 0.79 | 0.80 | 0.80 | 0.89 | 0.84 |
| 2*naphtoquinone | 0.45 | 0.29 | 0.18 | 0.15 | 0.19 | 0.21 | 0.20 | 0.20 | 0.11 | 0.16 |

ID-[Zn]-ID

Figure S33.Structure of ID-[Zn]-ID.

Figure S34.Image of the optimized structure of ID-[Zn]-ID.

H-4   (-0.21555)

H-3  (-0.20831)

H-2  (-0.20195)

H-1  (-0.19791)

HOMO  (-0.18020)

LUMO  (-0.11063)

L+1  (-0.10122)

L+2  (-0.08816)

L+3 (-0.08473)

L+4  (-0.04211)

Figure S35. Representations of the frontier MOs ofID-[Zn]-ID.The MO energies are in Hartree.

Table S17.Computed positions of the electronic transitions, oscillator strength (f), andmajor contributions of the ID-[Zn]-ID.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 768.2 | 2.3488 | HOMO→LUMO (97%) |
| 647.4 | 0.0076 | HOMO→L+1 (98%) |
| 620.4 | 0.0039 | H-1→LUMO (60%), HOMO→L+3 (-36%) |
| 574.9 | 0.0287 | H-3→L+1 (-11%), H-2→LUMO (85%) |
| 561.4 | 0.0001 | H-1→L+3 (-10%), HOMO→L+2 (85%) |
| 552.1 | 0.1152 | H-3→LUMO (59%), H-2→L+1 (-20%) |
| 527.6 | 0.0002 | H-7→L+1 (-10%), H-6→L+1 (-10%), H-5→LUMO (-18%), H-4→LUMO (39%) |
| 525.0 | 0.0002 | H-1→L+1 (100%) |
| 522.1 | 0.2425 | H-1→LUMO (33%), H-1→L+2 (18%), HOMO→L+3 (39%) |
| 518.5 | 0.0762 | H-7→LUMO (20%), H-6→LUMO (19%), H-4→L+1 (-13%), H-2→L+1 (-11%) |
| 495.5 | 0.0002 | H-3→LUMO (28%), H-2→L+1 (56%) |
| 484.9 | 0.0028 | H-6→LUMO (22%), H-5→LUMO (38%), H-4→LUMO (31%) |
| 476.6 | 0.0169 | H-3→L+1 (46%) |
| 475.7 | 0.0553 | H-7→LUMO (46%), H-6→LUMO (-27%) |
| 450.7 | 1.759 | H-11→LUMO (13%), H-1→L+3 (43%) |
| 445.4 | 0.0001 | H-8→LUMO (17%), H-4→LUMO (-12%), H-3→L+1 (18%) |
| 439.7 | 0.6742 | H-1→L+2 (64%), HOMO→L+3 (-18%) |
| 438.3 | 0.0089 | H-7→LUMO (18%), H-6→LUMO (11%), H-5→L+1 (-10%), H-4→L+1 (41%) |
| 436.2 | 0.0014 | H-8→LUMO (-17%), H-2→L+2 (72%) |
| 432.5 | 0.0004 | H-8→LUMO (24%), H-6→L+1 (17%), H-5→L+1 (-16%), H-2→L+3 (18%) |
| 431.2 | 0.003 | H-9→LUMO (24%), H-5→L+1 (10%), H-2→L+3 (38%) |
| 428.4 | 0.0038 | H-9→LUMO (-25%), H-8→LUMO (-21%), H-2→L+3 (35%) |
| 427.9 | 0.0016 | H-6→L+1 (33%), H-5→L+1 (26%), H-4→L+1 (21%) |
| 425.3 | 0.018 | H-10→LUMO (72%) |
| 419.9 | 0.0001 | H-7→L+1 (64%), H-6→L+1 (-13%) |
| 414.6 | 0.0114 | H-13→LUMO (45%), H-11→LUMO (21%) |
| 411.6 | 0.016 | H-13→LUMO (35%), H-11→LUMO (-16%), H-3→L+2 (24%) |
| 407.2 | 0.0908 | H-6→L+3 (10%), H-3→L+2 (28%), H-3→L+3 (19%) |
| 401.2 | 0.0541 | H-6→L+3 (13%), H-5→L+3 (30%), H-4→L+3 (29%) |
| 399.9 | 0.1104 | H-12→LUMO (22%), H-3→L+3 (-16%) |
| 399.8 | 0.1157 | H-12→LUMO (19%), H-6→L+3 (11%), H-3→L+3 (16%) |
| 391.6 | 0.0456 | H-11→LUMO (21%), H-9→L+1 (-10%), H-8→L+1 (40%) |
| 390.9 | 0.0027 | H-6→L+2 (13%), H-5→L+2 (31%), H-4→L+2 (50%) |
| 388.1 | 0.1246 | H-14→LUMO (25%), H-7→L+3 (16%), H-6→L+3 (-11%), H-3→L+3 (13%) |
| 386.7 | 0.0091 | H-6→L+2 (53%), H-5→L+2 (-18%) |
| 385.6 | 0.0026 | H-15→LUMO (31%), H-9→L+1 (15%), H-5→L+2 (11%), H-4→L+2 (-15%) |
| 384.9 | 0.0094 | H-15→LUMO (49%) |
| 384.7 | 0.0183 | H-14→LUMO (22%), H-9→L+1 (-14%), H-8→L+1 (-13%), H-5→L+2 (16%), H-4→L+2 (-14%) |
| 382.8 | 0.0865 | H-14→LUMO (20%), H-9→L+1 (22%), H-3→L+3 (-11%) |
| 382.0 | 0.0166 | H-10→L+1 (64%) |
| 378.5 | 0.0036 | H-19→LUMO (-11%), H-16→LUMO (20%), H-12→LUMO (32%) |
| 377.4 | 0.0603 | H-7→L+2 (65%) |
| 374.4 | 0.0143 | H-19→L+1 (17%), H-18→LUMO (-16%), H-11→LUMO (-14%) |
| 372.0 | 0.0001 | H-5→L+3 (-32%), H-4→L+3 (54%) |
| 371.0 | 0.0014 | H-11→L+1 (-18%), HOMO→L+4 (49%) |
| 368.5 | 0.0494 | H-7→L+3 (58%), H-6→L+3 (20%) |
| 364.1 | 0.0044 | H-16→LUMO (17%), H-11→L+1 (20%), H-8→L+3 (12%), HOMO→L+4 (29%) |
| 362.6 | 0.0008 | H-11→L+1 (-14%), H-9→L+3 (17%), H-8→L+3 (44%) |
| 361.5 | 0.0088 | H-13→L+3 (84%) |
| 357.1 | 0.0094 | H-10→L+3 (29%), H-9→L+3 (-10%) |
| 357.0 | 0.0019 | H-23→LUMO (-12%), H-10→L+3 (20%) |
| 355.7 | 0.0385 | H-24→LUMO (27%), H-23→L+1 (-26%) |
| 355.0 | 0.0001 | H-9→L+2 (14%), H-8→L+2 (69%) |
| 352.0 | 0.0059 | H-10→L+2 (-18%), H-9→L+2 (56%) |
| 351.3 | 0.0049 | H-10→L+2 (64%) |
| 349.7 | 0.0007 | H-10→L+3 (11%), H-9→L+3 (41%), H-8→L+3 (-31%) |
| 349.1 | 0.0006 | H-13→L+1 (95%) |
| 348.8 | 0.1346 | H-18→LUMO (14%), H-17→LUMO (23%), H-12→L+1 (34%) |
| 347.9 | 0.0107 | H-24→L+1 (11%), H-23→LUMO (-13%), H-16→LUMO (33%) |
| 344.6 | 0.0055 | H-17→LUMO (32%), H-12→L+1 (-32%) |
| 339.7 | 0.0002 | H-14→L+1 (96%) |
| 337.7 | 0.0009 | H-15→L+1 (96%) |
| 335.0 | 0.0606 | H-13→L+2 (10%), H-11→L+2 (74%) |
| 331.6 | 0.0838 | H-20→LUMO (-16%), H-17→LUMO (21%), H-16→L+1 (-11%) |
| 331.3 | 0.0268 | H-13→LUMO (12%), H-13→L+2 (74%), H-11→L+2 (-10%) |
| 328.3 | 0.0132 | H-14→L+3 (73%), H-11→L+3 (12%) |
| 327.0 | 0.0262 | H-15→L+3 (20%), H-12→L+3 (-17%), H-11→L+3 (28%) |
| 326.9 | 0.0059 | H-16→L+3 (11%), H-15→L+3 (21%), H-12→L+3 (26%), H-1→L+4 (10%) |
| 326.7 | 0.0283 | H-15→L+3 (-29%), H-11→L+3 (43%) |
| 324.9 | 0.0002 | H-22→LUMO (14%), H-21→LUMO (26%), H-20→LUMO (45%) |
| 324.2 | 0.0003 | H-22→LUMO (-34%), H-21→LUMO (52%) |
| 321.8 | 0.0007 | H-12→L+3 (-12%), H-1→L+4 (65%) |
| 321.6 | 0.0062 | H-22→LUMO (10%), H-18→LUMO (-12%), H-16→L+1 (64%) |
| 321.0 | 0 | H-25→LUMO (56%) |
| 320.8 | 0.0004 | H-26→LUMO (55%), H-24→LUMO (-11%) |
| 320.1 | 0.0015 | H-15→L+3 (19%), H-12→L+2 (56%) |
| 318.7 | 0.0249 | H-14→L+2 (86%) |
| 316.8 | 0 | H-15→L+2 (78%), H-12→L+3 (10%) |
| 313.5 | 0.0006 | H-19→LUMO (17%), H-18→L+1 (37%), H-16→L+2 (11%) |
| 310.1 | 0.0184 | H-20→LUMO (-16%), H-19→L+1 (40%), H-18→LUMO (15%) |
| 309.4 | 0 | H-20→L+1 (-15%), H-19→LUMO (16%), H-18→L+1 (10%), H-17→L+1 (33%) |
| 309.0 | 0.0001 | H-19→LUMO (-14%), H-17→L+1 (47%) |
| 305.3 | 0.0101 | H-2→L+4 (89%) |
| 301.9 | 0 | H-27→LUMO (25%), H-16→L+3 (55%), H-12→L+3 (-11%) |
| 300.1 | 0 | H-21→L+1 (35%), H-20→L+1 (48%) |
| 299.6 | 0 | H-22→L+1 (-31%), H-21→L+1 (49%) |
| 298.9 | 0.0445 | H-22→L+1 (13%), H-17→L+3 (-20%), H-16→L+2 (44%) |
| 298.7 | 0.0883 | H-18→L+3 (14%), H-17→L+3 (51%), H-16→L+2 (18%) |
| 297.5 | 0.0025 | H-28→LUMO (-19%), H-25→LUMO (17%), H-23→LUMO (21%), H-22→L+1 (16%) |
| 294.4 | 0.1884 | H-31→LUMO (-10%), H-17→L+2 (11%), HOMO→L+5 (55%) |
| 293.6 | 0.0692 | H-31→LUMO (29%), H-28→L+1 (-13%), H-18→L+2 (10%), HOMO→L+5 (19%) |
| 293.1 | 0.0086 | H-24→LUMO (29%), H-23→L+1 (37%) |
| 292.4 | 0.0001 | H-3→L+4 (65%) |
| 291.4 | 0.0004 | H-27→LUMO (50%), H-16→L+3 (-17%) |
| 291.3 | 0.0037 | H-18→L+2 (13%), H-17→L+2 (64%) |
| 290.8 | 0.0011 | H-28→LUMO (18%), H-24→L+1 (26%), H-3→L+4 (-18%) |
| 289.2 | 0.0017 | HOMO→L+6 (83%) |
| 286.5 | 0.0001 | H-29→LUMO (90%) |
| 285.9 | 0.0001 | H-30→LUMO (87%) |
| 285.4 | 0.0012 | H-6→L+4 (19%), H-5→L+4 (33%), H-4→L+4 (42%) |

Figure S36.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for ID-[Zn]-ID.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S18.Atomic contributions for the frontier MO for ID-[Zn]-ID.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2* porphyrins | 0.43 | 0.19 | 0.14 | ~1.00 | 0.74 | 0.40 | 0.07 | 0.54 | ~1.00 | 0.78 |
| 2*isoindigo | 0.57 | 0.81 | 0.86 | ~0.0 | 0.26 | 0.60 | 0.93 | 0.46 | ~0.0 | 0.22 |

NQ-[S]-[Zn]-[S]-NQ

Figure S37.Structure of NQ-[S]-[Zn]-[S]-NQ.

Figure S38.Image of the optimized structure of NQ-[S]-[Zn]-[S]-NQ.

H-4   (-0.21270)

H-3  (-0.20301)

H-2  (-0.19815)

H-1  (-0.19590)

HOMO  (-0.17723)

LUMO  (-0.10913)

L+1  (-0.10404)

L+2  (-0.09719)

L+3 (-0.08485)

L+4  (-0.06476)

Figure S39. Representations of the frontier MOs of NQ-[S]-[Zn]-[S]-NQ.The MO energies are in Hartree.

Table S19.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the NQ-[S]-[Zn]-[S]-NQ.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 785.6 | 3.1605 | HOMO→LUMO (95%) |
| 688.2 | 0.0081 | HOMO→L+1 (98%) |
| 628.8 | 0.0873 | HOMO→L+2 (93%) |
| 620.0 | 0.0013 | H-2→LUMO (-39%), HOMO→L+3 (51%) |
| 594.9 | 0.0309 | H-3→L+1 (-10%), H-1→LUMO (86%) |
| 567.7 | 0.6192 | H-3→LUMO (-37%), H-1→L+1 (45%) |
| 535.5 | 0.0159 | H-5→L+1 (20%), H-4→LUMO (33%), H-3→L+1 (-18%) |
| 531.7 | 0.0744 | H-5→LUMO (-13%), H-4→L+1 (-18%), H-3→LUMO (17%), H-1→L+1 (31%) |
| 525.8 | 0.1653 | H-2→LUMO (55%), H-2→L+2 (-17%), HOMO→L+3 (22%) |
| 522.4 | 0.0008 | H-2→L+1 (98%) |
| 521.1 | 0.078 | H-5→LUMO (18%), H-3→LUMO (33%), H-1→L+1 (11%) |
| 515.9 | 0.0155 | H-8→LUMO (11%), H-3→L+1 (18%), H-1→L+2 (39%) |
| 491.7 | 0.0008 | H-3→L+1 (-34%), H-1→L+2 (50%) |
| 484.9 | 0.733 | H-8→L+1 (-13%), H-7→LUMO (15%), H-3→L+2 (26%), H-2→L+3 (-14%) |
| 477.0 | 0.0031 | H-6→LUMO (66%), H-4→LUMO (-16%) |
| 473.0 | 0.5046 | H-7→LUMO (-16%), H-2→L+2 (38%), HOMO→L+3 (12%) |
| 469.7 | 0.0029 | H-8→LUMO (28%), H-6→LUMO (-19%), H-4→LUMO (-25%), H-3→L+1 (-11%) |
| 463.8 | 0.3149 | H-7→LUMO (27%), H-5→LUMO (17%), H-2→L+2 (25%), HOMO→L+3 (12%) |
| 452.8 | 0.0008 | H-1→L+3 (95%) |
| 451.8 | 0.3624 | H-9→LUMO (-13%), H-8→L+1 (10%), H-4→L+1 (-21%), H-3→L+2 (38%) |
| 450.3 | 0.0011 | HOMO→L+4 (83%) |
| 447.2 | 0.3463 | H-5→LUMO (-20%), H-4→L+1 (24%), H-2→L+3 (17%) |
| 438.6 | 0.001 | H-8→LUMO (-16%), H-5→L+1 (41%), H-4→LUMO (-17%), H-4→L+2 (-10%) |
| 433.4 | 0.2686 | H-7→LUMO (-12%), H-6→L+1 (-13%), H-5→LUMO (10%), H-2→L+3 (24%), HOMO→L+5 (10%) |
| 430.9 | 0.0362 | H-6→L+1 (80%) |
| 426.1 | 0.0002 | H-8→LUMO (21%), H-7→L+1 (63%) |
| 423.5 | 0.0002 | H-10→LUMO (80%) |
| 421.2 | 0.0048 | H-11→LUMO (-21%), H-9→LUMO (42%), H-8→L+1 (15%) |
| 420.0 | 0 | H-5→L+1 (14%), H-4→L+2 (49%) |
| 416.2 | 0.0059 | H-6→L+2 (43%) |
| 415.7 | 0.1631 | H-11→LUMO (-20%), H-5→L+2 (29%) |
| 413.4 | 0.2258 | H-3→L+3 (63%) |
| 412.8 | 0.0118 | H-6→L+2 (34%), H-4→L+2 (16%) |
| 412.2 | 0.0873 | H-11→LUMO (12%), H-7→L+2 (22%), H-5→L+2 (30%) |
| 410.0 | 0.0302 | H-14→LUMO (50%), H-14→L+2 (22%), H-13→LUMO (12%) |
| 404.7 | 0.151 | H-14→LUMO (12%), H-11→LUMO (18%), H-7→L+2 (-11%), HOMO→L+5 (30%) |
| 402.7 | 0.0006 | H-6→L+3 (85%) |
| 401.7 | 0.0039 | H-8→L+1 (-11%), H-7→L+2 (42%), H-5→L+2 (-10%) |
| 399.9 | 0.0001 | H-12→LUMO (-15%), H-9→L+1 (17%), H-8→L+2 (29%) |
| 395.9 | 0.047 | H-7→L+3 (38%), H-5→L+3 (21%), H-3→L+3 (-15%) |
| 391.0 | 0 | H-9→L+1 (44%), H-8→L+2 (-43%) |
| 387.5 | 0.0074 | H-10→L+1 (89%) |
| 385.6 | 0.0259 | H-9→L+2 (15%), HOMO→L+5 (19%) |
| 383.0 | 0.0005 | H-17→LUMO (25%), H-12→LUMO (33%) |
| 382.3 | 0 | H-16→LUMO (40%), H-16→L+2 (11%), H-4→L+3 (-33%) |
| 380.0 | 0.0148 | H-15→LUMO (70%), H-15→L+2 (17%) |
| 379.2 | 0.0018 | H-11→L+1 (52%), H-4→L+3 (-11%) |
| 378.5 | 0.2524 | H-9→L+2 (31%), H-1→L+4 (37%) |
| 378.2 | 0.0088 | H-16→LUMO (-19%), H-11→L+1 (-18%), H-4→L+3 (-18%), H-2→L+4 (28%) |
| 376.3 | 0.2238 | H-9→L+2 (26%), H-1→L+4 (-23%) |
| 375.3 | 0.0001 | H-16→LUMO (13%), H-10→L+2 (-14%), H-4→L+3 (15%), H-2→L+4 (47%) |
| 373.9 | 0.0003 | H-10→L+2 (71%), H-2→L+4 (14%) |
| 369.4 | 0.0069 | H-20→L+1 (13%), H-17→LUMO (42%), H-12→LUMO (-11%) |
| 368.3 | 0.0829 | H-11→L+3 (-14%), H-9→L+3 (24%), H-7→L+3 (-12%), H-5→L+3 (34%) |
| 367.6 | 0.0202 | H-13→LUMO (35%), H-12→L+1 (-23%), H-11→L+2 (28%) |
| 364.7 | 0.0003 | H-10→L+3 (90%) |
| 363.3 | 0.0124 | H-12→L+1 (33%), H-11→L+2 (41%) |
| 362.2 | 0.002 | H-14→L+3 (69%) |
| 360.9 | 0.0032 | H-13→L+1 (25%), H-12→L+2 (-12%), H-3→L+4 (21%) |
| 359.7 | 0.0016 | H-14→L+3 (-22%), H-9→L+3 (14%), H-7→L+3 (24%), H-5→L+3 (-16%) |
| 357.1 | 0 | H-8→L+3 (84%) |
| 355.9 | 0.0247 | H-9→L+3 (13%), H-1→L+4 (10%) |
| 353.6 | 0.0002 | H-28→L+1 (21%), H-27→LUMO (24%), H-27→L+2 (-11%), H-26→L+1 (13%), H-3→L+4 (12%) |
| 352.8 | 0.0073 | H-28→LUMO (13%), H-27→L+1 (28%) |
| 350.2 | 0.0065 | H-12→L+2 (27%), H-3→L+4 (43%), HOMO→L+6 (10%) |
| 348.9 | 0.0005 | H-14→L+1 (10%), H-13→L+1 (38%), H-12→L+2 (36%) |
| 347.0 | 0.0005 | H-14→L+1 (81%) |
| 343.0 | 0.0207 | H-11→L+3 (19%), H-9→L+3 (14%), H-2→L+5 (57%) |
| 342.8 | 0.0021 | HOMO→L+6 (70%) |
| 342.4 | 0.0716 | H-18→LUMO (51%), H-18→L+2 (11%), H-17→L+1 (-10%) |
| 341.4 | 0.0106 | H-14→LUMO (-22%), H-14→L+2 (40%), H-13→L+2 (29%) |
| 339.4 | 0.0177 | H-17→L+1 (30%), H-14→L+2 (-23%), H-13→L+2 (21%) |
| 338.8 | 0.0003 | H-15→L+1 (92%) |
| 337.4 | 0.0003 | H-1→L+5 (76%) |
| 337.2 | 0.001 | H-16→L+1 (90%) |
| 335.4 | 0.2546 | H-11→L+3 (-34%), H-9→L+3 (-21%), H-2→L+5 (35%) |
| 333.6 | 0.0239 | H-17→L+1 (47%), H-13→L+2 (-27%) |
| 331.4 | 0.0002 | H-17→L+3 (28%), H-16→LUMO (-14%), H-16→L+2 (31%), H-12→L+3 (20%) |
| 330.3 | 0.0174 | H-15→LUMO (-16%), H-15→L+2 (63%) |
| 330.1 | 0.0106 | H-17→LUMO (-13%), H-17→L+2 (37%), H-16→L+3 (11%) |
| 328.0 | 0.0178 | H-15→L+3 (73%), H-4→L+4 (11%) |
| 327.5 | 0.0003 | H-17→L+3 (-20%), H-16→L+2 (43%), H-12→L+3 (-23%) |
| 326.0 | 0.002 | H-15→L+3 (-12%), H-4→L+4 (63%) |
| 325.0 | 0.0008 | H-21→LUMO (11%), H-19→LUMO (28%), H-16→L+3 (41%) |
| 323.2 | 0.0007 | H-6→L+4 (50%), H-5→L+4 (-33%) |
| 322.9 | 0.0003 | H-6→L+4 (39%), H-5→L+4 (42%) |
| 322.4 | 0 | H-19→LUMO (15%), H-17→L+2 (35%), H-16→L+3 (-35%) |
| 321.4 | 0.0354 | H-19→L+1 (10%), H-4→L+4 (-11%), H-3→L+5 (37%) |
| 318.8 | 0.0005 | H-22→LUMO (82%) |
| 318.5 | 0.0016 | H-7→L+4 (76%) |
| 318.2 | 0.0002 | H-23→LUMO (80%) |
| 317.1 | 0.0569 | H-24→LUMO (12%), H-19→L+1 (-14%), H-3→L+5 (43%) |
| 316.3 | 0.0229 | H-26→LUMO (10%), H-24→LUMO (69%) |
| 316.1 | 0.0003 | H-17→L+3 (-40%), H-12→L+3 (51%) |
| 315.9 | 0.0014 | H-25→LUMO (83%) |
| 313.1 | 0.002 | H-29→LUMO (-31%), H-8→L+4 (37%) |
| 312.7 | 0.0013 | H-30→LUMO (23%), H-29→LUMO (19%), H-8→L+4 (25%) |
| 312.4 | 0.0013 | H-30→LUMO (39%), H-8→L+4 (-17%) |
| 310.2 | 0.0768 | H-13→L+3 (86%) |
| 309.1 | 0.0001 | H-21→LUMO (-16%), H-20→L+1 (12%), H-19→LUMO (15%), H-19→L+2 (21%) |

Figure S40.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for NQ-[S]-[Zn]-[S]-NQ.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S20.Atomic contributions for the frontier MO for NQ-[S]-[Zn]-[S]-NQ.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2* thiopene-porphyrins | 0.23 | 0.28 | ~1.00 | 0.46 | 0.90 | 0.52 | 0.12 | 0.54 | ~1.00 | 0.82 |
| 2*isoindigo | 0.77 | 0.72 | ~0.0 | 0.54 | 0.10 | 0.48 | 0.88 | 0.46 | ~0.0 | 0.18 |

ID-[B-Zn]-ID

Figure S41.Structure of ID-[B-Zn]-ID.

Figure S42.Image of the optimized structure of ID-[B-Zn]-ID.

H-4   (-0.21462)

H-3  (-0.20780)

H-2  (-0.20043)

H-1  (-0.18018)

HOMO  (-0.17426)

LUMO  (-0.10838)

L+1  (-0.10147)

L+2  (-0.08638)

L+3 (-0.08205)

L+4  (-0.04297)

Figure S43.Representations of the frontier MOs of ID-[B-Zn]-ID.The MO energies are in Hartree.

Table S21.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the ID-[B-Zn]-ID.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 806.4 | 0.1133 | HOMO→LUMO (96%) |
| 755.5 | 1.7423 | H-1→LUMO (93%) |
| 724.8 | 0.0011 | HOMO→L+1 (100%) |
| 653.0 | 0.0006 | H-1→L+1 (98%) |
| 614.8 | 0.0458 | H-1→L+3 (-23%), HOMO→L+2 (75%) |
| 602.2 | 0.7821 | H-1→L+2 (35%), HOMO→L+3 (55%) |
| 571.1 | 0.0002 | H-3→L+1 (-11%), H-2→LUMO (84%) |
| 550.6 | 0.2305 | H-3→LUMO (47%), H-2→L+1 (-26%), H-1→L+2 (11%) |
| 526.2 | 0.0008 | H-7→L+1 (-15%), H-6→L+1 (-11%), H-5→LUMO (25%), H-4→LUMO (30%) |
| 519.6 | 0.2018 | H-7→LUMO (24%), H-6→LUMO (17%), H-5→L+1 (-13%), H-4→L+1 (-13%), H-2→L+1 (-15%) |
| 500.7 | 0.629 | H-2→L+1 (29%), H-1→L+2 (31%), HOMO→L+3 (-22%) |
| 494.7 | 1.0347 | H-1→L+3 (68%), HOMO→L+2 (23%) |
| 490.7 | 0.6947 | H-3→LUMO (35%), H-2→L+1 (18%), HOMO→L+3 (10%) |
| 481.5 | 0 | H-8→LUMO (13%), H-5→LUMO (-15%), H-3→L+1 (34%) |
| 474.9 | 0.0011 | H-5→LUMO (-32%), H-4→LUMO (41%), H-3→L+1 (-14%) |
| 469.7 | 0.0519 | H-7→LUMO (-36%), H-6→LUMO (56%) |
| 448.7 | 0.0011 | H-8→LUMO (34%), H-5→LUMO (14%), H-3→L+1 (-26%) |
| 438.7 | 0 | H-8→LUMO (-10%), H-2→L+2 (85%) |
| 436.3 | 0.0152 | H-4→L+1 (70%) |
| 432.1 | 0.0097 | H-7→LUMO (10%), H-5→L+1 (77%) |
| 431.3 | 0 | H-6→L+1 (78%) |
| 430.8 | 0.0022 | H-9→LUMO (-14%), H-2→L+3 (74%) |
| 425.1 | 0.0634 | H-10→LUMO (58%), H-8→L+1 (-10%) |
| 424.8 | 0.0031 | H-9→LUMO (41%), H-8→LUMO (22%), H-7→L+1 (-14%), H-2→L+3 (14%) |
| 420.7 | 0 | H-9→LUMO (27%), H-7→L+1 (47%) |
| 414.6 | 0.0681 | H-11→LUMO (33%), H-10→LUMO (-32%), H-8→L+1 (-10%) |
| 407.4 | 0.042 | H-3→L+2 (85%) |
| 406.5 | 0.0056 | H-13→LUMO (18%), H-12→LUMO (47%) |
| 403.5 | 0 | H-13→LUMO (-27%), H-12→LUMO (40%) |
| 401.2 | 0.0028 | H-11→LUMO (14%), H-8→L+1 (58%) |
| 397.8 | 0.1122 | H-6→L+3 (27%), H-3→L+3 (66%) |
| 393.1 | 0.0048 | H-5→L+2 (-10%), H-5→L+3 (-33%), H-4→L+2 (12%), H-4→L+3 (36%) |
| 392.7 | 0.0015 | H-14→LUMO (81%) |
| 392.6 | 0.0023 | H-5→L+2 (-20%), H-5→L+3 (13%), H-4→L+2 (32%), H-4→L+3 (-15%), HOMO→L+4 (16%) |
| 390.3 | 0.0472 | H-4→L+2 (-14%), HOMO→L+4 (71%) |
| 388.2 | 0.0101 | H-9→L+1 (76%) |
| 387.1 | 0.0001 | H-15→LUMO (-22%), H-13→LUMO (12%), H-10→L+1 (52%) |
| 387.0 | 0.0053 | H-6→L+2 (73%) |
| 386.8 | 0.0003 | H-15→LUMO (38%), H-10→L+1 (37%) |
| 384.7 | 0.0209 | H-21→LUMO (13%), H-16→LUMO (26%), H-11→LUMO (-18%) |
| 383.1 | 0.0476 | H-7→L+3 (-21%), H-6→L+3 (46%), H-3→L+3 (-27%) |
| 381.5 | 0.0001 | H-5→L+2 (54%), H-4→L+2 (34%) |
| 376.2 | 0.0071 | H-19→LUMO (20%), H-7→L+2 (55%) |
| 375.8 | 0.0174 | H-17→LUMO (81%) |
| 375.3 | 0.0003 | H-1→L+4 (63%) |
| 374.9 | 0.0396 | H-19→LUMO (45%), H-16→LUMO (10%), H-7→L+2 (-21%) |
| 371.7 | 0 | H-15→LUMO (14%), H-13→LUMO (24%), H-11→L+1 (40%) |
| 369.4 | 0.1054 | H-18→LUMO (55%), H-12→L+1 (19%) |
| 368.4 | 0.0023 | H-18→LUMO (-13%), H-12→L+1 (72%) |
| 368.0 | 0.0074 | H-8→L+3 (10%), H-5→L+3 (41%), H-4→L+3 (36%) |
| 367.2 | 0.1895 | H-21→LUMO (-17%), H-16→LUMO (42%) |
| 365.2 | 0.0018 | H-21→L+1 (-12%), H-20→LUMO (15%), H-11→L+1 (11%), H-1→L+4 (23%) |
| 361.8 | 0.0155 | H-7→L+3 (69%), H-6→L+3 (21%) |
| 361.5 | 0.0033 | H-11→L+1 (-10%), H-8→L+2 (77%) |
| 359.2 | 0.0016 | H-9→L+3 (21%), H-8→L+3 (57%) |
| 357.8 | 0.0534 | H-13→L+1 (65%) |
| 356.0 | 0.0025 | H-14→L+1 (86%) |
| 354.9 | 0.0001 | H-30→L+1 (11%), H-29→LUMO (-16%), H-27→L+1 (-14%), H-26→LUMO (24%) |
| 354.3 | 0.0029 | H-10→L+2 (25%), H-10→L+3 (55%) |
| 354.1 | 0.0019 | H-30→LUMO (-10%), H-29→L+1 (17%), H-27→LUMO (15%), H-26→L+1 (-14%), H-24→LUMO (-10%) |
| 353.9 | 0.0019 | H-9→L+2 (64%), HOMO→L+5 (11%) |
| 352.8 | 0.0033 | H-10→L+2 (67%), H-10→L+3 (-24%) |
| 350.2 | 0.0055 | H-9→L+2 (-18%), H-9→L+3 (42%), H-8→L+3 (-19%) |
| 348.8 | 0.0001 | H-9→L+3 (-15%), HOMO→L+5 (56%) |
| 347.2 | 0.0717 | H-15→L+1 (79%) |
| 345.9 | 0.009 | H-17→L+1 (93%) |
| 344.7 | 0.0002 | H-16→L+1 (79%) |
| 341.2 | 0.0016 | H-12→L+2 (72%) |
| 339.7 | 0.0001 | H-18→L+1 (-20%), H-13→L+2 (10%), H-12→L+3 (48%) |
| 338.1 | 0.005 | H-1→L+5 (34%), HOMO→L+7 (47%) |
| 338.0 | 0.0072 | HOMO→L+6 (90%) |
| 337.5 | 0 | H-18→L+1 (69%), H-12→L+3 (19%) |
| 337.2 | 0.0472 | H-11→L+2 (83%) |
| 334.2 | 0.0099 | H-19→L+3 (-18%), H-14→L+3 (54%) |
| 333.6 | 0.0001 | H-26→LUMO (-12%), H-19→L+1 (65%) |
| 333.6 | 0.0193 | H-19→L+3 (58%), H-14→L+3 (19%), H-11→L+3 (13%) |
| 331.8 | 0.0444 | H-1→L+5 (-40%), HOMO→L+7 (45%) |
| 331.3 | 0.0004 | H-14→L+2 (66%), H-11→L+3 (-10%) |
| 329.8 | 0.0002 | H-26→LUMO (18%), H-22→LUMO (10%), H-19→L+1 (26%), H-13→L+2 (-13%) |
| 328.3 | 0.001 | H-15→L+3 (38%), H-13→L+3 (-32%) |
| 327.8 | 0.0141 | H-30→LUMO (-10%), H-24→LUMO (18%), H-23→LUMO (-17%), H-1→L+6 (-17%) |
| 327.5 | 0.0017 | H-22→LUMO (26%), H-13→L+2 (22%) |
| 325.8 | 0.0007 | H-29→LUMO (13%), H-26→LUMO (17%), H-13→L+2 (33%) |
| 325.1 | 0.0275 | H-19→L+3 (-15%), H-14→L+2 (17%), H-11→L+3 (54%) |
| 324.2 | 0.0023 | H-27→LUMO (11%), HOMO→L+8 (43%) |
| 323.7 | 0.0221 | H-30→LUMO (-19%), H-27→LUMO (-10%), HOMO→L+8 (36%) |
| 322.3 | 0.0001 | H-17→L+3 (36%), H-1→L+7 (48%) |
| 320.6 | 0.0258 | H-23→LUMO (-17%), H-1→L+6 (55%) |
| 319.6 | 0.0132 | H-17→L+2 (73%), H-13→L+3 (16%) |
| 318.3 | 0.0009 | H-15→L+2 (59%), H-1→L+7 (17%) |
| 318.0 | 0.0004 | H-16→L+2 (67%) |
| 315.7 | 0.0003 | H-25→LUMO (81%), H-22→LUMO (-12%) |
| 315.4 | 0.0353 | H-24→LUMO (22%), H-23→LUMO (31%), H-18→L+3 (-10%) |
| 314.9 | 0.0484 | H-18→L+3 (55%), H-1→L+8 (-16%) |
| 314.3 | 0.008 | H-19→LUMO (-11%), H-19→L+2 (55%) |
| 314.1 | 0.0096 | H-17→L+3 (42%), H-1→L+7 (-25%) |
| 313.7 | 0.0258 | H-15→L+3 (42%), H-13→L+3 (28%) |
| 313.4 | 0.0852 | H-16→L+3 (71%), H-11→L+3 (11%) |
| 312.8 | 0.0801 | H-18→L+2 (71%) |
| 312.1 | 0.0041 | H-2→L+4 (66%) |

Figure S44.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for ID-[B-Zn]-ID.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S22.Atomic contributions for the frontier MO for ID-[B-Zn]-ID.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Benzo-porphyrins | 0.55 | 0.21 | 0.22 | 0.76 | 0.99 | 0.34 | 0.08 | 0.65 | 0.99 | 0.77 |
| 2*isoindigo | 0.45 | 0.79 | 0.78 | 0.24 | 0.01 | 0.66 | 0.92 | 0.35 | 0.01 | 0.23 |

ID-[S]-[B-Zn]-[S]-ID

Figure S45.Structure of ID-[S]-[B-Zn]-[S]-ID.

Figure S46.Image of the optimized structure of ID-[S]-[B-Zn]-[S]-ID.

H-4   (-0.21146)

H-3  (-0.20248)

H-2  (-0.19472)

H-1  (-0.17809)

HOMO  (-0.17460)

Figure S47.Representations of the frontier MOs ofID-[S]-[B-Zn]-[S]-ID.The MO energies are in Hartree.

LUMO  (-0.10726)

L+1  (-0.10412)

L+2  (-0.09496)

L+3 (-0.08241)

L+4  (-0.06564)

Table S23.Computed positions of the electronic transitions, oscillator strength (f), and major contributions of the ID-[S]-[B-Zn]-[S]-ID.

| Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- |
| 770.2 | 0.3003 | HOMO→LUMO (88%) |
| 758.4 | 2.3379 | H-1→LUMO (86%) |
| 716.3 | 0.0004 | HOMO→L+1 (100%) |
| 682.3 | 0.0041 | H-1→L+1 (97%) |
| 659.2 | 0.0645 | H-1→L+3 (-13%), HOMO→L+2 (79%) |
| 635.6 | 0.1797 | H-1→L+2 (62%), HOMO→L+3 (27%) |
| 590.9 | 0.021 | H-3→L+1 (12%), H-2→LUMO (83%) |
| 577.7 | 1.6795 | H-3→LUMO (27%), H-2→L+1 (44%), HOMO→L+3 (12%) |
| 538.4 | 0.9125 | H-4→L+1 (10%), H-2→L+1 (-11%), H-1→L+2 (-19%), HOMO→L+3 (38%) |
| 535.4 | 0.0139 | H-5→L+1 (17%), H-4→LUMO (34%), H-3→L+1 (-18%) |
| 532.6 | 0.0126 | H-5→LUMO (11%), H-4→L+1 (17%), H-3→LUMO (-18%), H-2→L+1 (29%) |
| 516.6 | 0.7905 | H-1→L+3 (78%), HOMO→L+2 (17%) |
| 513.6 | 0.0209 | H-8→LUMO (-17%), H-3→L+1 (21%), H-2→L+2 (31%) |
| 511.9 | 0.1979 | H-8→L+1 (-18%), H-3→LUMO (38%) |
| 494.8 | 0.0004 | H-3→L+1 (-25%), H-2→L+2 (60%) |
| 472.7 | 0.0041 | H-8→LUMO (10%), H-4→LUMO (31%), H-3→L+1 (12%), HOMO→L+4 (27%) |
| 472.2 | 0.0085 | H-4→LUMO (-12%), HOMO→L+4 (70%) |
| 468.4 | 0.0524 | H-7→LUMO (25%), H-5→LUMO (-20%), H-4→L+1 (-11%) |
| 464.5 | 0.0009 | H-6→LUMO (71%), H-6→L+2 (-11%) |
| 455.5 | 0.0192 | H-7→LUMO (13%), H-5→LUMO (-26%), H-4→L+1 (27%) |
| 452.9 | 0.2076 | H-3→L+2 (79%) |
| 452.5 | 0.0013 | H-1→L+4 (90%) |
| 449.8 | 0.0083 | H-2→L+3 (89%) |
| 437.5 | 0.0015 | H-5→L+1 (58%), H-4→LUMO (-14%) |
| 436.0 | 0.0706 | H-9→LUMO (18%), H-7→LUMO (17%), H-6→L+1 (19%), H-5→LUMO (11%), H-4→L+1 (-16%) |
| 434.0 | 0.0065 | H-6→L+1 (76%) |
| 426.0 | 0.0002 | H-7→L+1 (56%) |
| 423.8 | 0.0019 | H-10→LUMO (22%), H-8→LUMO (27%), H-4→L+2 (-11%) |
| 423.5 | 0.0884 | H-3→L+3 (11%), HOMO→L+5 (85%) |
| 418.0 | 0.0019 | H-10→LUMO (11%), H-6→L+2 (-29%), H-4→L+2 (42%) |
| 416.6 | 0.1433 | H-9→LUMO (-22%), H-8→L+1 (34%) |
| 414.9 | 0.1301 | H-11→LUMO (26%), H-9→LUMO (-18%) |
| 414.6 | 0.0252 | H-10→LUMO (33%), H-6→L+2 (15%) |
| 413.2 | 0.0313 | H-7→L+2 (-20%), H-5→L+2 (44%) |
| 412.9 | 0.0028 | H-6→L+2 (35%), H-4→L+2 (18%) |
| 407.7 | 0.3576 | H-3→L+3 (57%), H-1→L+5 (11%) |
| 406.9 | 0.0712 | H-11→LUMO (-29%), H-3→L+3 (-15%), H-1→L+5 (33%) |
| 399.5 | 0.0001 | H-9→L+1 (38%), H-8→L+2 (11%) |
| 398.9 | 0.0017 | H-7→L+2 (50%), H-5→L+2 (17%) |
| 397.3 | 0.0016 | H-13→LUMO (66%), H-13→L+2 (-18%) |
| 395.5 | 0.0186 | H-11→LUMO (10%), H-1→L+5 (31%) |
| 394.5 | 0.0037 | H-6→L+3 (83%) |
| 392.3 | 0.0041 | H-10→L+1 (89%) |
| 391.5 | 0.0006 | H-9→L+1 (-17%), H-8→L+2 (65%) |
| 389.1 | 0.0077 | H-7→L+3 (42%), H-5→L+3 (-39%) |
| 386.2 | 0.0001 | H-16→LUMO (35%), H-12→LUMO (-19%) |
| 384.4 | 0.0037 | H-15→LUMO (69%), H-15→L+2 (-20%) |
| 383.5 | 0.0318 | H-11→L+1 (73%) |
| 383.4 | 0.4771 | H-2→L+4 (70%) |
| 379.6 | 0.0034 | H-9→L+2 (70%) |
| 378.6 | 0.0014 | H-10→L+2 (-20%), H-4→L+3 (49%) |
| 376.6 | 0.0031 | H-10→L+2 (37%), H-4→L+3 (22%) |
| 374.9 | 0.0032 | H-16→LUMO (-19%), H-12→LUMO (-15%), H-10→L+2 (26%) |
| 372.9 | 0.0544 | H-12→L+1 (26%), H-11→L+2 (-14%) |
| 370.5 | 0.0004 | H-14→LUMO (41%), H-12→L+1 (32%) |
| 369.6 | 0.0027 | H-17→LUMO (66%), H-17→L+2 (-16%) |
| 369.0 | 0.0398 | H-21→LUMO (26%), H-21→L+2 (-19%), H-14→LUMO (10%), H-13→L+1 (12%), H-11→L+2 (-12%) |
| 367.4 | 0.0115 | H-13→L+1 (77%) |
| 366.5 | 0.0022 | H-14→L+1 (19%), H-3→L+4 (23%), H-2→L+5 (12%) |
| 366.2 | 0.0102 | H-21→LUMO (10%), H-11→L+2 (46%) |
| 362.2 | 0.0362 | H-20→LUMO (-13%), H-11→L+3 (-11%), H-9→L+3 (18%), H-7→L+3 (16%), H-5→L+3 (21%) |
| 361.1 | 0.0537 | H-20→LUMO (28%), H-19→LUMO (-12%), H-7→L+3 (10%), H-5→L+3 (10%) |
| 360.5 | 0.0215 | H-10→L+3 (54%), HOMO→L+6 (-22%) |
| 358.7 | 0.0281 | H-15→L+1 (12%), H-10→L+3 (18%), HOMO→L+6 (43%) |
| 357.4 | 0.0002 | H-15→L+1 (-13%), H-13→LUMO (14%), H-13→L+2 (52%) |
| 356.4 | 0.0067 | H-14→L+1 (-33%), H-3→L+4 (33%) |
| 356.3 | 0.0127 | H-20→LUMO (11%) |
| 355.0 | 0.0028 | H-18→LUMO (16%) |
| 354.6 | 0.0014 | H-11→L+3 (37%), H-9→L+3 (-22%), H-7→L+3 (21%), H-5→L+3 (15%) |
| 354.3 | 0.0033 | H-15→L+1 (-19%), H-12→L+2 (26%), H-1→L+6 (14%) |
| 353.7 | 0.0007 | H-15→L+1 (-13%), H-1→L+6 (-16%), HOMO→L+7 (53%) |
| 353.2 | 0.0041 | H-15→L+1 (23%), H-13→L+2 (11%), H-12→L+2 (17%), HOMO→L+7 (12%) |
| 351.6 | 0.0084 | H-10→L+3 (-11%), H-8→L+3 (54%) |
| 351.4 | 0.0344 | H-16→L+1 (64%) |
| 351.1 | 0.0014 | H-18→LUMO (-11%), H-12→L+2 (18%) |
| 350.3 | 0.0024 | H-32→L+1 (11%), H-19→LUMO (26%) |
| 346.5 | 0.0007 | H-17→L+1 (44%), H-15→LUMO (-10%), H-15→L+2 (-39%) |
| 345.0 | 0.0012 | H-2→L+5 (63%), H-1→L+6 (13%) |
| 343.2 | 0.0008 | H-17→L+1 (53%), H-15→LUMO (13%), H-15→L+2 (26%) |
| 342.5 | 0.001 | H-16→LUMO (11%), H-16→L+2 (41%), H-13→L+3 (22%) |
| 341.0 | 0.0086 | H-14→L+2 (51%), H-11→L+3 (11%), H-9→L+3 (13%) |
| 340.9 | 0.004 | H-14→L+2 (24%), H-11→L+3 (-21%), H-9→L+3 (-24%) |
| 340.5 | 0.0049 | H-18→LUMO (-10%), H-1→L+6 (36%), HOMO→L+7 (10%) |
| 339.0 | 0.0132 | H-18→L+1 (51%) |
| 338.7 | 0.0431 | H-1→L+7 (58%), HOMO→L+6 (-11%) |
| 336.9 | 0.0017 | H-19→L+1 (65%) |
| 336.4 | 0.0012 | H-20→L+1 (66%), H-13→L+3 (20%) |
| 334.6 | 0.0189 | H-17→LUMO (14%), H-17→L+2 (48%), H-16→L+3 (10%), H-1→L+7 (-13%) |
| 334.1 | 0.0007 | H-20→L+1 (-19%), H-16→L+2 (-23%), H-13→L+3 (39%) |
| 334.1 | 0.006 | H-15→L+3 (41%), H-4→L+4 (30%) |
| 333.6 | 0 | H-18→L+1 (-10%), H-15→L+3 (-30%), H-4→L+4 (32%) |
| 331.7 | 0.0011 | H-17→L+2 (-20%), H-16→L+3 (20%), H-12→L+3 (-19%), HOMO→L+8 (26%) |
| 330.1 | 0.0568 | H-21→L+3 (79%) |
| 329.1 | 0.0002 | H-16→L+3 (-13%), H-12→L+3 (12%), HOMO→L+8 (66%) |
| 328.2 | 0.0002 | H-21→L+1 (90%) |
| 327.3 | 0.0247 | H-6→L+4 (64%), H-5→L+4 (10%), H-3→L+5 (-14%) |
| 326.8 | 0.0032 | H-7→L+4 (-11%), H-5→L+4 (63%) |
| 326.4 | 0.1173 | H-20→L+2 (14%), H-19→L+2 (-11%), H-6→L+4 (14%), H-4→L+4 (13%), H-3→L+5 (22%) |
| 325.5 | 0.0118 | H-20→L+2 (34%), H-3→L+5 (-23%) |
| 324.8 | 0.0241 | H-20→L+2 (-19%), HOMO→L+9 (-17%), HOMO→L+10 (29%) |

Figure S48.Bar graph (blue) reporting the position of the electronic transitions vs the oscillator strength (f) for ID-[S]-[B-Zn]-[S]-ID.The black line represents a spectrum where 1000 cm-1 is applied to each transition.

Table S24.Atomic contributions for the frontier MO for ID-[S]-[B-Zn]-[S]-ID.

|  | H-4 | H-3 | H-2 | H-1 | H | L | L+1 | L+2 | L+3 | L+4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2*Thiopene- Benzo-porphyrins | 0.29 | 0.31 | 0.52 | 0.91 | ~1.00 | 0.38 | 0.12 | 0.70 | ~1.00 | 0.82 |
| 2*isoindigo | 0.71 | 0.69 | 0.48 | 0.09 | ~0.0 | 0.62 | 0.88 | 0.30 | ~0.0 | 0.18 |