Supporting information

Photodegradation of naphthalene over Fe3O4 under visible light

| Code | Intermediates | m/z+ |
| --- | --- | --- |
| 1 | 1,2-diphenyl butadiene | 91, 104, 117, 129, 193, 207 |
| 2 | 1,4-diphenyl butadiene | 32, 44, 65, 77, 91, 103, 115, 130, 165, 179, 194, 206 |
| 3 | 1,3-diphenyl propane | 40, 51, 77, 91, 101, 115, 128, 165, 178, 191, 206) |
| 4 | 1,2-diphenyl cyclopropane | 51, 65, 77, 91, 101, 115, 142, 165, 179, 191, 194 |
| 5 | 1,4-diphenylbutene-1 | 65, 77, 91, 104, 117, 129, 131 |
| 6 | benzyl succinic acid | 65, 77, 91, 103, 117, 129, 179, 194, 207 |
| 7 | 1,3-diphenyl acrylketone | 32, 45, 73, 91, 103, 115, 178, 193, 207, 219 |
| 8 | (benzyl methyl ether)-ethyl diacetate | 65, 77, 91, 104, 117, 194, 207, 267 |
| 9 | hydroxyethyl methyl ketone | 15, 31, 43, 61, 70, 88 |
| 10 | 2-ethoxy ethyl ether | 40, 51, 65, 77, 92, 105, 117 |
| 11 | ethyl acetate | 29, 43, 61, 70, 88 |

irradiation

Jiawei Zhang, Shanshan Fan, Bin Lu, Qinghai Cai*, Jingxiang Zhao, Shuying Zang*

Table SI1 Data of GC-MS measurement for reaction byproducts

Fig SI1 The sample solution before (2) and after (1) reaction