Electronic Supplementary Material

Nitrogen and chlorine co-doped carbon dots as probe for sensing and imaging in biological samples

Jin Lia,1, Kai Tangb,1, Jianxin Yub, Hanqin Wangb, Mingli Tub, Xiaobo Wanga,b*

a  Department of reproductive medicine, Suizhou Hospital, Hubei University of

Medicine, 60 Longmen Street, Suizhou 441300, China

b  Center for translational medicine, Suizhou Hospital, Hubei University of Medicine,

8 east central park road, Suizhou 441300, China

1  These authors contributed equally to this work

*Corresponding Author

Xiaobo Wang

Tel:86-0722-3252551

Fax:86-0722-3252400

E-mail: wangxiaobo78@126.com

Figures, Tables.

Fig. S1  TEM images (a) of Orn-CDs (inset: the HRTEM image of the Orn-CDs) ,

and the corresponding SAED image (b) and XRD patterns of Orn-CDs (c).

Fig. S2  FTIR spectra of the prepared Orn-CDs.

Fig. S3  XPS survey spectra (a), high resolution XPS spectra of C 1s (b), N 1s (c), O 1s

(d) of the prepared Orn-CDs.

Fig. S4  The influence of pH value, concentrations of Orn-CDs, incubation time of

Orn-CDs based sensing system on the detection of Fe3+ and ascorbic acid.

Table S1 Comparison of Orn-CDs and other carbon dots based probes for Fe3+ detection.

Fig. S5   Selectivity of Orn-CDs toward different metal ions.

Fig. S6   Photographs of Orn-CDs upon addition of Fe3+and ascorbic acid.

Fig. S7   Fluorescence spectrum of Orn-CDs before and after addition of ascorbic acid.

Table S2  Comparison of Orn-CDs and other probes for ascorbic acid detection.

Fig.S8   Selectivity of Orn-CDs/Fe3+ system toward ascorbic acid.

Fig. S9   UV-vis spectrum of Orn-CDs in the presence of Fe3+and ascorbic acid.

Fig. S10  Fluorsecence decays of the prepared Orn-CDs upon addition of Fe3+.

Table S3  Double-exponential fitting of Orn-CDs and Orn-CDs /Fe3+ decay curves.

Table S4  Fe3+ determination results in human serum and urine samples.

Table S5  Ascorbic acid determination results in human urine samples.

Fig. S11  Viability of the prepared Orn-CDs against A549 cells.

Fig. S1  TEM images (a) of Orn-CDs (inset: the HRTEM image of the Orn-CDs),

and the corresponding SAED image (b) and XRD patterns of Orn-CDs (c).

Fig. S2 FTIR spectra of the prepared Orn-CDs.

Fig. S3  (a) XPS survey spectra, high resolution XPS spectra of C 1s (b), N 1s (c), O 1s (d) of the prepared Orn-CDs

Fig. S4 (a) The influence of pH value (3.0-8.0) of Tris-HCl solution (20 mmol L-1) on the Orn-CDs (0.15 mg mL-1) fluorescence quenching efficiency (Effq, black line) by 200 µmol L-1 Fe3+ and Orn-CDs (0.15 mg mL-1)/Fe3+ (200 µmol L-1) platform fluorescence recovering efficiency (Effr, red line) after addition of 50 µmol L-1 ascorbic acid. (b) The effect of concentrations of Orn-CDs (from left to right : 0.05, 0.10, 0.15, 0.20, 0.25 mg mL-1) on the fluorescence quenching efficiency (Effq, black line) by 200 µmol L-1 Fe3+ and Orn-CDs (0.15 mg mL-1)/Fe3+ (200 µmol L-1) platform fluorescence recovering efficiency (Effr, red line) after addition of 50 µmol L-1 ascorbic acid. (c) Time dependent FL response of 0.15 mg/ml Orn-CDs to 20 µmol L-1 Fe3+ in Tris-HCl solution at room temperature. (d) Time dependent fluorescence response of 0.15 mg mL-1 of Orn-CDs /200 µmol L-1 of Fe3+ to 10 µmol L-1 ascorbic acid in Tris-HCl solution at room temperature.

Table S1 Comparison of Orn-CDs and other carbon dots based probes for Fe3+ detection

| samples | linear range (µmol L-1) | detection limit (µmol L-1) | ref |
| --- | --- | --- | --- |
| water samples human serum, urine | — 0.3-546 | 0.01 0.09 | 1 2 |
| water samples | 0.11-4.46 | 0.05 | 3 |
| water samples water samples drinking and tap water tap water,fruits | — — — 25-200 | 10 10 0.29 0.05882 | 4 5 6 7 |
| water, urine | 0.05-10.0 | 0.0137 | 8 |
| human serum, urine | 0.3-50.0 | 0.0956 | this work |

Fig. S5  Selectivity of Orn-CDs toward different metal ions. The concentration of Orn-CDs is 0.15 mg mL-1 in Tris-HCl solution, 50 µmol L-1 for Fe3+ and 2 mmol L-1 for other metal ions.

Fig. S6  Photographs of Orn-CDs (5 mg mL-1) (left), Orn-CDs(5 mg mL-1) + Fe3+(10 mmol L-1 (middle), and Orn-CDs(5 mg mL-1) + Fe3+ (10 mmol L-1) + ascorbic acid (10 mmol L-1) (right).

Fig. S7 Fluorescence spectra of 0.15 mg mL-1 of Orn-CDs before and after additon of ascorbic acid (10 µmol L-1).

Table S2 Comparison of Orn-CDs and other probes for ascorbic acid detection

| samples | linear range (µmol L-1) | detection limit (µmol L-1) | ref |
| --- | --- | --- | --- |
| fruits human urine juice human serum human blood plasma water human urine | 25-300 0.2-11.0 1-90 0.15-15.0 1.5-10 8-100 0.5-10.0 | 0.236 0.01 0.018 0.105 0.2 2.4 0.137 | 7 8 9 10 11 12 this work |

Fig. S8  Selectivity of Orn-CDs/Fe3+ system toward ascorbic acid. The concentration of Orn-CDs is 0.15 mg mL-1 in Tris-HCl solution, 200 µmol L-1 of Fe3+and 10 µmol L-1 of ascorbic acid .The concentration of other interference analytes is 100 µmol L-1.

Fig. S9  UV-vis spectra of the prepared Orn-CDs (0.15 mg mL-1, black line), 0.15 mg mL-1 Orn-CDs/200 µmol L-1 of Fe3+ (red line), and 0.15 mg mL-1 Orn-CDs/200 µmol L-1 Fe3+/AA (blue line for 10 µmol L-1 AA, green line for 20 µmol L-1 AA, purple line for 50 µmol L-1 AA respectively)

Fluorescence decay curves were performed in a time–correlated-single-photo- counting (TCSPC) system from FL980 spectrometer under excitation at 326 nm. Data were fit by using the bi-exponential function in equation (1).

(1)

α1 and α2 were the fractional contributions of time-resolved decay lifetime of  τ1and τ2.

Fig. S10 Fluorescence decays of the prepared Orn-CDs (0.15 mg mL-1, black curve) upon addition of 100 µmol L-1 Fe3+ (red curve) at excitation/emission wavelengths (λex/λem) of 326/404 nm.

Table S3.  Double-exponential fitting of Orn-CDs and Orn-CDs /Fe3+ decay curves.

| Sample name | Orn-CDs | Orn-CDs /Fe3+ |
| --- | --- | --- |
| τ1(ns)/A1 (%) | 3.5841/36.3 | 2.4074/21.24 |
| τ2(ns)/A2 (%) | 12.4129/63.7 | 8.6186/78.76 |
| Average τ (ns) | 9.21 | 7.30 |

Table S4. Fe3+ determination results in human serum and urine samples.

| Sample | Added (µmol L-1) | Found (µmol L-1) | Recovery (%, n=3) | RSD (%, n=3) |
| --- | --- | --- | --- | --- |
| Serum | 0.50 | 0.542 | 108.4 | 2.41 |
|  | 5.00 | 5.126 | 102.5 | 3.80 |
|  | 20.00 50.00 | 18.811 53.837 | 94.1 107.7 | 1.48 2.30 |
| Urine | 0.50 | 0.480 | 95.9 | 1.59 |
|  | 5.00 | 4.921 | 98.4 | 3.67 |
|  | 20.00 50.00 | 20.468 53.236 | 102.3 106.5 | 2.17 3.75 |

Table S5. Ascorbic acid determination results in human urine samples.

| Sample | Added (µmol L-1) | Found (µmol L-1) | Recovery (%, n=3) | RSD (%, n=3) |
| --- | --- | --- | --- | --- |
| Urine 1 | 0.50 | 0.470 | 94.0 | 2.21 |
|  | 2.00 | 1.887 | 94.4 | 3.10 |
|  | 5.00 10.00 | 5.166 9.878 | 103.3 98.8 | 2.12 3.16 |
| Urine 2 | 0.50 | 0.474 | 94.9 | 2.07 |
|  | 2.00 | 2.136 | 106.8 | 2.78 |
|  | 5.00 10.00 | 4.831 10.490 | 96.6 104.9 | 3.47 2.66 |

Cell viability assay

The biocompatibility of Orn-CDs against A549 cells were investigated by MTT assay. After seeding A549 in 96-well plate at 1×104/well and cultured for 24 h at 37°C under 5% CO2, the supernatant was discarded and the cells were washed three times with PBS, subsequently, different concentration (0, 0.1, 0.2, 0.3, 0.4, 0.5, 0.6, 0.7, 0.8, 0.9, 1.0 mg mL-1 ) of the Orn-CDs in DMEM medium were added (100 μL/well) and clutured for furthe 24 h at 37°C. Finally, MTT (5 mg mL-1, 20 μL/well) was added and incubated for another 4 h. After removing the culture medium, DMSO (150 μL/well) was added and shaken at 37°C for 10 min. A microplate reader (Bio Tek Epoch) was used to measure the absorbance of each sample at 490 nm. The data represent the mean ± standard deviation of four independent experiments. The cell viability was expressed as the below formula:

cell viability%= ODtreatedODcontrol ×100%

where ODcontrol was acquired before addition of Orn-CDs and ODtreated was acquired in the presence of Orn-CDs.

Fig. S11  Viability of the prepared Orn-CDs against A549 cells.

References

1.	H. Huang, C. Li, S. Zhu, H. Wang, C. Chen, Z. Wang, T. Bai, Z. Shi and S. Feng, Langmuir, 2014, 30, 13542-13548. (doi:10.1021/la503969z)

2.	Y. Liu, W. Duan, W. Song, J. Liu, C. Ren, J. Wu, D. Liu and H. Chen, ACS applied materials & interfaces, 2017, 9, 12663-12672. (doi:10.1021/acsami.6b15746)

3.	P. Karfa, E. Roy, S. Patra, S. Kumar, A. Tarafdar, R. Madhuri and P. K. Sharma, RSC Advances, 2015, 5, 58141-58153. (doi:10.1039/c5ra09525e)

4.	G. He, M. Xu, M. Shu, X. Li, Z. Yang, L. Zhang, Y. Su, N. Hu and Y. Zhang, Nanotechnology, 2016, 27, 395706. (doi:10.1088/0957-4484/27/39/395706)

5.	Z. Wang, C. Xu, Y. Lu, X. Chen, H. Yuan, G. Wei, G. Ye and J. Chen, Sensors and Actuators B: Chemical, 2017, 241, 1324-1330. (doi:10.1016/j.snb.2016.09.186)

6.	H.-J. Cheng, C.-L. Kao, Y.-F. Chen, P.-C. Huang, C.-Y. Hsu and C.-H. Kuei, Microchimica Acta, 2017, 184, 3179-3187. (doi:10.1007/s00604-017-2336-7)

7.	F. Du, X. Gong, W. Lu, Y. Liu, Y. Gao, S. Shuang, M. Xian and C. Dong, Talanta, 2018, 179, 554-562. (doi:10.1016/j.talanta.2017.11.030)

8.	M. Shamsipur, K. Molaei, F. Molaabasi, M. Alipour, N. Alizadeh, S. Hosseinkhani and M. Hosseini, Talanta, 2018, 183, 122-130. (doi:10.1016/j.talanta.2018.02.042)

9.	X. Kong, Y. Gong and Z. Fan, Journal of fluorescence, 2016, 26, 1755-1762. (doi:10.1007/s10895-016-1867-3)

10.	W.-J. Niu, D. Shan, R.-H. Zhu, S.-Y. Deng, S. Cosnier and X.-J. Zhang, Carbon, 2016, 96, 1034-1042. (doi:10.1016/j.carbon.2015.10.051)

11.	X. Wang, P. Wu, X. Hou and Y. Lv, The Analyst, 2013, 138, 229-233. (doi:10.1039/c2an36112d)

12.     C. Mi, T. Wang, P. Zeng, S. Zhao, N. Wang and S. Xu, Analytical Methods, 2013, 5, 1463-1468. (doi:10.1039/c3ay26387h)